Cirlex ® Polyimide Film

Order Online at www.professionalplastics.com

| TYPICAL PROPERTIES of CIRLEX POLYIMIDE FILMS (at 73°F) |
| --- |
| ASTM or UL test | Property | Cirlex ® 900CL 0.009" (.23mm) | Cirlex ®1200CL 0.012" (.31mm) | Cirlex ®1500CL 0.015" (.38mm) | Cirlex ®3000CL 0.030" (.76mm) | Cirlex ®5000CL 0.050" (1.27mm) |
| PHYSICAL |
| D792 | Density (lb/in³) (g/cm³) | 0.051 1.42 | 0.051 1.42 | 0.051 1.42 | 0.051 1.42 | 0.051 1.42 |
| D570 | Water Absorption, saturation (%) | 4.0 | 4.0 | 4.0 | 4.0 | 4.0 |
| MECHANICAL |
| D638 | Tensile Strength (psi) | 32,490 | 34,000 | 35,000 | 33,300 | 31,800 |
| D638 | Yield Point at 3% (psi) | 6,100 | 6,500 | 7,800 | 7,100 | 6,100 |
| D638 | Stress to Produce 5% Elongation (psi) | 10,300 | 10,800 | 11,200 | 10,370 | 9,400 |
| D790 | Ultimate Elongation (%) | 65 | 64 | 63 | 57 | 56 |
| D790 | Tensile Modulus (psi) | 330,000 | 332,000 | 334,000 | 274,000 | 264,000 |
| THERMAL |
| - | Glass Transition Temp (°F / °C) | 664 / 351 | 664 / 351 | 664 / 351 | 664 / 351 | 664 / 351 |
| D696 | Coefficient of Linear Thermal Expansion (x 10-5 in./in./°F) | 11 | 11 | 11 | 11 | 11 |
| C177 | Thermal Conductivity (BTU-in/ft²-hr-°F) (x 10-4 cal/cm-sec-°C) | 0.0025 0.084 | 0.0025 0.084 | 0.0025 0.084 | 0.0025 0.084 | 0.0025 0.084 |
| C177 | Specific Heat (J/g-°K) | 1.09 | 1.09 | 1.09 | 1.09 | 1.09 |
| UL94 | Flammability Rating | V-0 | V-0 | V-0 | V-0 | V-0 |
| ELECTRICAL |
| D149 | Dielectric Strength (V/mil) short time | 2790 | 2000 | 1940 | 1270 | arc |
| D150 | Dielectric Constant at 1 kHz | 3.45 | 3.55 | 3.58 | 3.74 | 3.72 |
| D150 | Dissipation Factor | 0.0021 | 0.0020 | 0.0018 | 0.0023 | 0.0026 |

NOTE: The information contained herein are typical values intended for reference and comparison purposes only. They should NOT be used as a basis for design specifications or quality control. Contact us for manufacturers' complete material property datasheets.
All values at 73°F (23°C) unless otherwise noted.

KAPTON, CIRLEX and VESPEL are registered trademarks of DuPont.