Duratron® XP (CM), Polyimide, high purity, unfilled, compression molded

Material Notes: Duratron XP is a compression-molded polyimide that offers high purity, high strength, high heat resistance, and good machinability. These properties, combined with its chemical resistance and dimensional stability, make Duratron XP ideal for components in semiconductor manufacturing and test equipment.

| MECHANICAL PROPERTIES | ENGLISH VALUES | COMMENTS | METRIC VALUES |
| --- | --- | --- | --- |
| Specific Gravity | 1.4 | ASTM D792 | 1.4 |
| Tensile Strength, psi | 16000 | ASTM D638 | 110 MPa |
| Tensile Modulus, psi | 583000 | ASTM D638 | 4,020 MPa |
| Elongation, % | 4 | ASTM D638 | 4 % |
| Flexural Strength, psi | 20000 | ASTM D790 | 138 MPa |
| Flexural Modulus, psi | 600000 | ASTM D790 | 4,137 MPa |
| Compressive Strength, psi | 24000 | ASTM D695, 10% Def. | 165 MPa |
| Compressive Modulus, psi | 450000 | ASTM D695 | 3,103 MPa |
| Hardness, Rockwell M | 110 | ASTM D785 | 110 |
| Izod Impact (Notched), ft-lb/in | 1.4 | ASTM D256 Type A | 75 J/m |
| Coefficient of Friction, Dynamic | 0.23 | Dry vs. Steel, QTM55007 | 0.23 |
| Limiting PV, psi-fpm | 32500 | 4:1 safety factor; QTM 55007 | 1.1 MPa-m/sec |
| k (wear) factor, 10-10in3-min/lb-ft-hr | 50 | QTM 55010 | 50 10-10in3-min/lb-ft-hr |
| Relative Machinability | 5 | 1-10, 1=Easier to Machine | 5 |
| THERMAL PROPERTIES | ENGLISH VALUES | COMMENTS | METRIC VALUES |
| Coefficient of Thermal Expansion, 10E-4/°F | 0.27 | ASTM E831 (-40°F to 300°F) | 0.49 10-4/K |
| Deflection Temperature 264 psi, ºF | 680 | ASTM D648 | 360 °C |
| Tg-Glass Transition (Amorphous), ºF | 613 | ASTM D3418 | 323 °C |
| Continuous Service in Air (Max), °F | 580 | Long Term | 304 °C |
| Thermal Conductivity, BTU-in/hr-ft²-°F | 1.53 | ASTM F433 | 0.22 W/m-K |
| ELECTRICAL PROPERTIES | VALUES | COMMENTS | METRIC VALUES |
| Dielectric Strength, Short Term, Volts/mil | 700 | ASTM D149 | 28 kV/mm |
| Surface Resistance, Ohm/Square | 1E+13 | Lower Limit; EOS/ESD S11.11 | 1E+13 Ohm/Square |
| Dielectric Constant, 1 MHz | 3.41 | ASTM D150 | 3.41 |
| Dissipation Factor, 1 MHz | 0.0038 | ASTM D150 | 0.0038 |
| CHEMICAL PROPERTIES | ENGLISH VALUES | COMMENTS | METRIC VALUES |
| Water Absorption Immersion, 24 hr., % | 0.4 | ASTM D570(2) | 0.4 % |
| Water Absorption Immersion Sat, % | 1.3 | ASTM D570(2) | 1.3 % |
| Acids, Weak (acetic, dilute HCl) | 3 | Acceptable Service | 3 |
| Acids, Strong (conc. HCl or sulfuric) | 2 | Limited Service | 2 |
| Alkalies, Weak (dilute NaOH) | 2 | Limited Service | 2 |
| Alkalies, Strong (conc. NaOH) | 1 | Unacceptable | 1 |
| Hydrocarbons, Aromatic (toluene) | 3 | Acceptable Service | 3 |
| Hydrocarbons, Aliphatic (gasoline) | 3 | Acceptable Service | 3 |
| Ketones, Esters (acetone) | 3 | Acceptable Service | 3 |
| Ethers (diethyl ether, THF) | 3 | Acceptable Service | 3 |
| Chlorinated Solvents (methylene chloride) | 3 | Acceptable Service | 3 |
| Alcohols (methanol, anti-freeze) | 3 | Acceptable Service | 3 |
| Continuous Sunlight | 2 | Limited Service | 2 |
| COMPLIANCE | ENGLISH VALUES | COMMENTS | METRIC VALUES |
| Flammability, UL94 (5=V-0; 4=V-1; 3=V-2; 1=HB) | 5 (V-0) | UL94; 1/8 inch | 5 |
| FDA (1=Yes) | 0 | Not Compliant | 0 |

Call Professional Plastics at (800) 966-7767 or

E-Mail sales@proplas.com

Order Online at www.professionalplastics.com