# Typical Properties of Imide Films

| Typical Properties of Imides: |
| --- |
| Properties | Units | Ultem® 1000-1000 | Ultem® CRS | Ultem® XHT 6050 | Aurum® 450C |
| Tensile Strength, yield | psi | 14,500 | 14,500 | 14,000 | 17,100 |
| Flexural Modulus | psi | 480,000 | 450,000 | 450,000 | 548,000 |
| Tensile Elongation, break | % | 60.0 | 60.0 | --- | 110 |
| Izod Impact, notched | ft-lb/in | 1.0 | 1.1 | 1.3 | 1.1 |
| Water Absorption, 24 hrs. | % | 0.25 | 0.25 | 0.15 | 0.30 |
| Specific Gravity | --- | 1.27 | 1.28 | 1.30 | 1.33 |
| Area Factor | in2/lb/mil | 21,834 | 21,645 | 21,322 | 20,833 |
| Flammability Rating | UL-94 | VTM-0 | VTM-0 | VTM-0 | VTM-0 |
| Glass Transition Temperature | °C | 215 | 220 | 249 | 250 |
| Natural Color | --- | amber | amber | amber | orange-amber |

# Text boxes

Need help with your order? Call us at 1-800-966-PROS 
or order online at www.professionalplastics.com today!