| TYPICAL PROPERTIES of Kel-F/PCTFE |
| --- |
| ASTM or UL test | Property | PCTFE |
| PHYSICAL |
| D792 | Density (lb/in³) (g/cm³) | 0.077 2.13 |
| D570 | Water Absorption, 24 hrs (%) | < 0.01 |
| MECHANICAL |
| D638 | Tensile Strength (psi) | 5,300 |
| D638 | Tensile Modulus (psi) | 207,000 |
| D638 | Tensile Elongation at Break (%) | 150 |
| D790 | Flexural Strength (psi) | 8,500 |
| D790 | Flexural Modulus (psi) | 180,000 |
| D695 | Compressive Strength (psi) | 5,500 |
| D695 | Compressive Modulus (psi) | 180,000 |
| D785 | Hardness, Shore D | D90 |
| D256 | IZOD Notched Impact (ft-lb/in) | 5 |
| THERMAL |
| D696 | Coefficient of Linear Thermal Expansion (x 10-5 in./in./°F) | 7.0 |
| D648 | Heat Deflection Temp (°F / °C) at 264 psi | 258 / 126 |
| D3418 | Melting Temp (°F / °C) | 415 / 212 |
| - | Max Operating Temp (°F / °C) | 270 / 132 |
| C177 | Thermal Conductivity (BTU-in/ft²-hr-°F) (x 10-4 cal/cm-sec-°C) | 1.45 4.99 |
| UL94 | Flammability Rating | V-0 |
| ELECTRICAL |
| D149 | Dielectric Strength (V/mil) short time, 1/8" thick | 500 |
| D150 | Dielectric Constant at 1 MHz | - |
| D150 | Dissipation Factor at 1 MHz | - |
| D257 | Volume Resistivity (ohm-cm)at 50% RH | 1018 |

NOTE: The information contained herein are typical values intended for reference and comparison purposes only. They should not be used as the sole basis for design specifications or quality control

All values at 73°F (23°C) unless otherwise noted.

KEL-F is a registered trademark of 3M Company.
NEOFLON is a registered trademark of Daikin Industries.

# Text boxes

Need help with your order? Call us at 1-800-966-PROS 
or order online at www.professionalplastics.com today!