Machine Grade ABS Material Data Sheet

| Physical Properties Metric English Comments Density 1.04 g/cc 0.0376 lb/in³ Grade Count = 3 Melt Flow 18 - 23 g/10 min 18 - 23 g/10 min Average = 21.3 g/10 min; Grade Count = 3 Mechanical Properties Hardness, Rockwell R 103 - 112 103 - 112 Average = 110; Grade Count = 3 Tensile Strength, Yield 42.5 - 44.8 MPa 6160 - 6500 psi Average = 44 MPa; Grade Count = 3 Elongation at Break 23 - 25 % 23 - 25 % Average = 24.3%; Grade Count = 3 Flexural Modulus 2.25 - 2.28 GPa 326 - 331 ksi Average = 2.3 GPa; Grade Count = 3 Flexural Yield Strength 60.6 - 73.1 MPa 8790 - 10600 psi Average = 68.9 MPa; Grade Count = 3 Izod Impact, Notched 2.46 - 2.94 J/cm 4.61 - 5.51 ft-lb/in Average = 2.8 J/cm; Grade Count = 3 Electrical Properties Arc Resistance 120 sec 120 sec Grade Count=1 Comparative Tracking Index 600 V 600 V Grade Count=1 Hot Wire Ignition, HWI 15 sec 15 sec Grade Count = 1 High Amp Arc Ignition, HAI 120 arcs 120 arcs Grade Count = 1 High Voltage Arc-Tracking Rate, HVTR 25 mm/min 0.984 in/min Grade Count = 1 Thermal Properties Maximum Service Temperature, Air 88 - 89 °C 190 - 192 °F Average = 88.7°C; Grade Count = 3 Deflection Temperature at 1.8 MPa (264 psi) 88 - 89 °C 190 - 192 °F Average = 88.7°C; Grade Count=3 Vicat Softening Point 100 °C 212 °F Grade Count = 1 Flammability, UL94 HB HB Grade Count = 3 |  |
| --- | --- |