Quadrant EPP Nylon 101, Unfilled, Type 66 nylon, extruded

Material Notes: 
Nylon 101 is an extruded form of polyamide, offering rigidity, strength, wear resistance, and heat resistance to 210°F. It is commonly used in both structural and general-purpose bearing and wear applications. This material is available in natural and black. The natural material is compliant with FDA, USDA, NST, and 3A-Dairy regulations.

| Physical Properties | Metric | English | Comments |
| --- | --- | --- | --- |
| Density | 1.15 g/cc | 0.0415 lb/in³ | ASTM D792 |
| Water Absorption | 0.3 % | 0.3 % | 24 hour immersion; ASTM D570 |
| Moisture Absorption at Equilibrium | 0.9 % | 0.9 % | Water Vapor Regained |
| Water Absorption at Saturation | 7 % | 7 % | Immersion; ASTM D570 |
| Outgassing - Total Mass Loss | 2.4 % | 2.4 % |  |
| Collected Volatile Condensable Material | 0 % | 0 % |  |
| Mechanical Properties |
| Hardness, Rockwell M | 85 | 85 | ASTM D785 |
| Hardness, Rockwell R | 115 | 115 | ASTM D785 |
| Hardness, Shore D | 80 | 80 | ASTM D2240 |
| Tensile Strength, Ultimate | 79.3 MPa | 11500 psi | ASTM D638 |
| Elongation at Break | 50 % | 50 % | ASTM D638 |
| Tensile Modulus | 2.93 GPa | 425 ksi | ASTM D638 |
| Flexural Modulus | 3.1 GPa | 450 ksi | ASTM D790 |
| Flexural Yield Strength | 103 MPa | 15000 psi | ASTM D790 |
| Compressive Yield Strength | 86.2 MPa | 12500 psi | 10% Deflection; ASTM D695 |
| Compressive Modulus | 2.9 GPa | 420 ksi | ASTM D695 |
| Machinability | 10 % | 10 % | QEPP 10 to 100 scale |
| Shear Strength | 68.9 MPa | 10000 psi | ASTM D732 |
| Coefficient of Friction | 0.25 | 0.25 | Dynamic; Dry vs. Steel; PTM55007 |
| K (wear) Factor | 80 | 80 | 10-10 in3-min/lb-ft-hr; PTM55007 |
| Limiting Pressure Velocity | 0.0946 MPa-m/sec | 2700 psi-ft/min | PTM55007 |
| Izod Impact, Notched | 0.32 J/cm | 0.6 ft-lb/in | ASTM D256A |
| Electrical Properties |
| Surface Resistivity per Square | 1e+013 ohm | 1e+013 ohm | EOS/ESD S11.11 |
| Dielectric Constant | 3.6 | 3.6 | 1 MHz; ASTM D150(2) |
| Dielectric Strength | 15.7 kV/mm | 400 V/mil | Short Term; ASTM D149(2) |
| Dissipation Factor | 0.02 | 0.02 | 1 MHz; ASTM D150(2) |
| Thermal Properties |
| CTE, linear 68°F | 99 µm/m-°C | 55 µin/in-°F | ASTM E831 (TMA) |
| Thermal Conductivity | 0.245 W/m-K | 1.7 BTU-in/hr-ft²-°F |  |
| Melting Point | 260 °C | 500 °F | ASTM D3418 |
| Maximum Service Temperature, Air | 98.9 °C | 210 °F | Continuous Service Without Load |
| Deflection Temperature at 1.8 MPa (264 psi) | 93.3 °C | 200 °F | ASTM D648 |
| Flammability, UL94 | V-2 | V-2 | UL94 |
| Descriptive Properties |
| Compliance - Canada AG | Not Compliant |  |
| Compliance - Dairy 3A | Compliant |  |
| Compliance - FDA | Compliant |  |
| Compliance - NSF | Compliant |  |
| Compliance - USDA | Compliant |  |
| Compliance - USP Class VI | Not Compliant |  |
| Service in Alcohols | Limited |  |
| Service in Aliphatic Hydrocarbons | Acceptable |  |
| Service in Aromatic Hydrocarbons | Acceptable |  |
| Service in Chlorinated Solvents | Limited |  |
| Service in Continuous Sunlight | Limited |  |
| Service in Ethers | Acceptable |  |
| Service in Inorganic Salt Solutions | Acceptable |  |
| Service in Ketones | Acceptable |  |
| Service in Steam | Limited |  |
| Service in Strong Acids | Unacceptable |  |
| Service in Strong Alkalies | Unacceptable |  |
| Service in Weak Acids | Limited |  |
| Service in Weak Alkalies | Limited |  |