Nylon 6 with 30% Glass-Fiber Filled

| Physical Properties Metric English Comments Density 1.17 - 1.62 g/cc 0.0423 - 0.0585 lb/in³ Average = 1.35 g/cc; Grade Count = 168 Water Absorption 0 - 7.5 % 0 - 7.5 % Average = 2.9%; Grade Count = 113 Moisture Absorption at Equilibrium 0.9 - 2.5 % 0.9 - 2.5 % Average = 1.9%; Grade Count = 68 Water Absorption at Saturation 1.8 - 8.2 % 1.8 - 8.2 % Average = 6.1%; Grade Count = 56 Linear Mold Shrinkage 0.0015 - 0.007 cm/cm 0.0015 - 0.007 in/in Average = 0.0033 cm/cm; Grade Count = 109 Linear Mold Shrinkage, Transverse 0.007 - 0.017 cm/cm 0.007 - 0.017 in/in Average = 0.009 cm/cm; Grade Count = 50 Melt Flow 4 - 145 g/10 min 4 - 145 g/10 min Average = 50.6 g/10 min; Grade Count = 14 Mechanical Properties Hardness, Rockwell E 55 55 Grade Count = 1 Hardness, Rockwell M 90 - 100 90 - 100 Average = 95; Grade Count = 2 Hardness, Rockwell R 110 - 121 110 - 121 Average = 120; Grade Count = 28 Tensile Strength, Ultimate 65 - 195 MPa 9430 - 28300 psi Average = 140 MPa; Grade Count = 130 Tensile Strength, Yield 95 - 195 MPa 13800 - 28300 psi Average = 140 MPa; Grade Count = 31 Elongation at Break 2 - 10 % 2 - 10 % Average = 4.5%; Grade Count = 154 Elongation at Yield 2 - 6 % 2 - 6 % Average = 3.7%; Grade Count = 18 Tensile Modulus 3.2 - 11.17 GPa 464 - 1620 ksi Average = 7.5 GPa; Grade Count = 105 Flexural Modulus 2.8 - 9.7 GPa 406 - 1410 ksi Average = 7.2 GPa; Grade Count = 95 Flexural Yield Strength 110 - 310 MPa 16000 - 45000 psi Average = 220 MPa; Grade Count = 96 Compressive Yield Strength 16 - 152 MPa 2320 - 22000 psi Average = 100 MPa; Grade Count=6 Poisson's Ratio 0.35 0.35 Grade Count = 15 Shear Strength 59 - 85 MPa 8560 - 12300 psi Average = 72 MPa; Grade Count = 2 Izod Impact, Notched 0.6 - 2.4 J/cm 1.12 - 4.5 ft-lb/in Average = 1.3 J/cm; Grade Count = 80 Izod Impact, Unnotched 6.4 - 11.7 J/cm 12 - 21.9 ft-lb/in Average = 9.4 J/cm; Grade Count = 7 Izod Impact, Notched Low Temp 0.5 - 1.37 J/cm 0.937 - 2.57 ft-lb/in Average = 0.916 J/cm; Grade Count = 25 Charpy Impact, Unnotched 4 - 11 J/cm² 19 - 52.4 ft-lb/in² Average = 8.6 J/cm²; Grade Count = 19 Charpy Impact, Notched Low Temp 0.56 - 1.5 J/cm² 2.67 - 7.14 ft-lb/in² Average = 0.987 J/cm²; Grade Count = 18 Charpy Impact, Unnotched Low Temp 3.5 - 9 J/cm² 16.7 - 42.8 ft-lb/in² Average = 7 J/cm²; Grade Count = 11 Charpy Impact, Notched 0.55 - 3.5 J/cm² 2.62 - 16.7 ft-lb/in² Average = 1.6 J/cm²; Grade Count = 28 Coefficient of Friction 0.16 0.16 Grade Count=1 Coefficient of Friction, Static 0.25 0.25 Grade Count=1 Tensile Creep Modulus, 1 hour 2400 - 7000 MPa 348000 - 1.02e+006 psi Average = 4700 MPa; Grade Count = 16 Tensile Creep Modulus, 1000 hours 2000 - 5000 MPa 290000 - 725000 psi Average = 3600 MPa; Grade Count = 16 Taber Abrasion, mg/1000 Cycles 15 15 Grade Count = 1 Electrical Properties Electrical Resistivity 430000 - 1e+015 ohm-cm 430000 - 1e+015 ohm-cm Average = 5E+14 ohm-cm; Grade Count = 89 Surface Resistance 55000 - 1e+016 ohm 55000 - 1e+016 ohm Average = 2E+14 ohm; Grade Count = 72 Dielectric Constant 3.2 - 10 3.2 - 10 Average = 4.6; Grade Count = 73 Dielectric Constant, Low Frequency 2.6 - 15 2.6 - 15 Average = 7.4; Grade Count = 52 Dielectric Strength 16 - 41 kV/mm 406 - 1040 kV/in Average = 34.6 kV/mm; Grade Count = 69 Dissipation Factor 0.005 - 0.36 0.005 - 0.36 Average = 0.065; Grade Count = 68 Dissipation Factor, Low Frequency 0.0035 - 3.4 0.0035 - 3.4 Average = 0.16; Grade Count = 59 Arc Resistance 60 - 136 sec 60 - 136 sec Average = 96.3 sec; Grade Count=26 Comparative Tracking Index 400 - 600 V 400 - 600 V Average = 540 V; Grade Count=44 Hot Wire Ignition, HWI 7 - 120 sec 7 - 120 sec Average = 55.4 sec; Grade Count = 14 High Amp Arc Ignition, HAI 60 - 120 arcs 60 - 120 arcs Average = 110 arcs; Grade Count = 14 High Voltage Arc-Tracking Rate, HVTR 0 - 10 mm/min 0 - 0.394 in/min Average = 8.6 mm/min; Grade Count = 14 Thermal Properties CTE, linear 20°C 19 - 100 µm/m-°C 10.6 - 55.6 µin/in-°F Average = 29.9 µm/m-°C; Grade Count=42 CTE, linear 20°C Transverse to Flow 65 - 150 µm/m-°C 36.1 - 83.3 µin/in-°F Average = 90.7 µm/m-°C; Grade Count=22 Heat Capacity 1.5 - 2.43 J/g-°C 0.359 - 0.581 BTU/lb-°F Average = 1.9 J/g-K; Grade Count = 3 Thermal Conductivity 0.17 - 0.5 W/m-K 1.18 - 3.47 BTU-in/hr-ft²-°F Average = 0.38 W/m-K; Grade Count = 7 Melting Point 210 - 255 °C 410 - 491 °F Average = 220°C; Grade Count = 118 Maximum Service Temperature, Air 110 - 232 °C 230 - 450 °F Average = 200°C; Grade Count = 99 Deflection Temperature at 0.46 MPa (66 psi) 174 - 221 °C 345 - 430 °F Average = 210°C; Grade Count=84 Deflection Temperature at 1.8 MPa (264 psi) 155 - 232 °C 311 - 450 °F Average = 200°C; Grade Count=124 Vicat Softening Point 183 - 220 °C 361 - 428 °F Average = 200°C; Grade Count = 33 UL RTI, Electrical 65 - 140 °C 149 - 284 °F Average = 110°C; Grade Count = 33 UL RTI, Mechanical with Impact 65 - 105 °C 149 - 221 °F Average = 86.8°C; Grade Count = 33 UL RTI, Mechanical without Impact 65 - 140 °C 149 - 284 °F Average = 110°C; Grade Count = 33 Flammability, UL94 HB HB Grade Count = 102 Oxygen Index 21 - 23 % 21 - 23 % Average = 22.4%; Grade Count = 8 Processing Properties Processing Temperature 235 - 282 °C 455 - 540 °F Average = 270°C; Grade Count = 59 Rear Barrel Temperature 227 - 260 °C 441 - 500 °F Average = 240°C; Grade Count = 8 Middle Barrel Temperature 235 - 260 °C 455 - 500 °F Average = 250°C; Grade Count = 8 Front Barrel Temperature 235 - 271 °C 455 - 520 °F Average = 260°C; Grade Count = 8 Nozzle Temperature 235 - 271 °C 455 - 520 °F Average = 260°C; Grade Count = 6 Mold Temperature 52 - 115 °C 126 - 239 °F Average = 91°C; Grade Count = 35 Drying Temperature 77 - 85 °C 171 - 185 °F Average = 84°C; Grade Count = 44 |  |
| --- | --- |