Nylon® – oil filled, Type 6

| Specific Gravity | 1.14 g/cm3 |
| --- | --- |
| Tensile Strength | 10,000 (psi) |
| Compressive Strength @ 10% Deflection | 14,000 - 15,000 (psi) |
| Elongation | 35 - 40 % |
| Tensile Modulus | 435,000 (psi) |
| Tensile Impact 73°F | 80 -130 ft. lbs./ in. |
| Flexural Strength | 13,000 (psi) |
| Flexural Modulus | 350,000 (psi) |
| Coefficient of Friction | .17 - .19 (dry vs. Steel) |
| 24 Hour H2O | .3 % |
| Equilibrium H2O | 1.0 - 2.8 % |
| Hardness | 80 (Scale D) |
| Coefficient of Thermal Expansion | 5.5 x 10 (-5) in./in./F |
| Continuous Operating Temp | 220 - 250 Degrees F |