Spirally Cut Tubing: Nylon

Nylon is suitable for self-extinguishing and does not produce any toxic or irritating byproducts, even when exposed to an open flame or excessive operating temperatures. Recommended for use in enclosed environments where the possibility of fire exists, this material is also lightweight, highly abrasion-resistant and operates over a wide temperature range. Also available in Black for outdoor use.

| Size |  | Outside Diameter O.D. | Nominal Dimensions Wall | Inside Diameter I.D. | Pitch | Maximum Bundle Range Inches | Weight Lbs/M Ft. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Nylon |
| 1/8" |  | 0.125 | 0.015 | 0.095 | 0.187 | 1/16 to 1/2 | 3 |
| 3/16" |  | 0.187 | 0.020 | 0.147 | 0.250 | 1/8 to 1 1/2 | 7 |
| 1/4" |  | 0.250 | 0.025 | 0.200 | 0.375 | 3/16 to 2 | 9 |
| 3/8" |  | 0.375 | 0.035 | 0.305 | 0.438 | 5/16 to 3 | 18 |
| 1/2" |  | 0.500 | 0.035 | 0.430 | 0.500 | 3/8 to 4 | 25 |
| 5/8" |  | 0.625 | 0.032 | 0.561 | 0.625 | 1/2 to 4 1/2 | 32 |
| 3/4" |  | 0.750 | 0.032 | 0.686 | 0.750 | 1/2 to 5 | 38 |
| 1" |  | 1.000 | 0.032 | 0.936 | 1.000 | 1 to 7 | 50 |
| Black Nylon |
| 1/8" |  | 0.125 | 0.015 | 0.095 | 0.187 | 1/16 to 1/2 | 3 |
| 3/16" |  | 0.187 | 0.020 | 0.147 | 0.250 | 1/8 to 1 1/2 | 7 |
| 1/4" |  | 0.250 | 0.025 | 0.200 | 0.375 | 3/16 to 2 | 9 |
| 3/8" |  | 0.375 | 0.035 | 0.305 | 0.438 | 5/16 to 3 | 18 |
| 1/2" |  | 0.500 | 0.035 | 0.430 | 0.500 | 3/8 to 4 | 25 |
| 5/8" |  | 0.625 | 0.032 | 0.561 | 0.625 | 1/2 to 4 1/2 | 32 |
| 3/4" |  | 0.750 | 0.032 | 0.686 | 0.750 | 1/2 to 5 | 38 |
| 1" |  | 1.000 | 0.032 | 0.936 | 1.000 | 1 to 7 | 50 |

Properties of Nylon

| Max-Min Operat Temp | Abrasion Resistance | Specific Gravity D792-66 | Effect of Solvents | Effect of Acids | Effect of Alkalies | Water Absorption % D-570 | Flammability | MIL Spec. & Approvals |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Nylon |
| 250°F 121°C | -40°F -40°C | 6-8 | 1.14 | None | Satisfactory except for strong acids | None | 1.5 | Self Extinguishing | MIL M-20693B Type I MIL M-22096A LP 410A MIL M-19098 |
| Black Nylon |
| 250°F 121°C | -40°F -40°C | 6-8 | 1.14 | None | Satisfactory except for strong acids | None | 1.5 | Self Extinguishing | MIL M-206393A Type II MIL M-22096 LP 410A MIL T-47287A Type II AS 1294 |