# PEEK TAPE DATA SHEET

## Product Description:

Extruded, virgin PEEK (polyethetherketone) film has been surface modified on one side and coated with an Acrylic or High Temperature Silicone adhesive.  The acrylic adhesive is resistant to high humidity and harsh chemical environments while retaining good peel strength with clean removal.  Silicone Adhesive has low residue upon removal and withstands temperatures from -100F to +450F.

The surface modification enhances bond strength to other materials.  Peel-off liner is applied to the adhesive side.  The untreated side is lubricious, abrasion resistant, and free of pin holes. Series #37-_A (Acrylic) or 37-_S (Silicone)

Performance & Application Information:

This tape has the best combination of friction and wear properties combined with high heat resistance (350F with Acrylic Adhesive; 450F with Silicone Adhesive), chemical resistance and electrical insulation.  Tapes can be used on many different hard mating surfaces such as steel, ceramic or glass.  Typical applications for the tape include sliding bearings, abrasion resistant wire wraps and oil field equipment requiring abrasion resistance and electrical insulation.

### TYPICAL PROPERTIES PEEK Tape with Adhesive

| Property | Test Method | Data |
| --- | --- | --- |
| Backing Material |  | VICTREX® PEEK Film |
| Backing Thickness |  | .002 |
| Adhesive System |  | Acrylic or Silicone |
| Adhesive Thickness (in) |  | .002", .005", .010" |
| Adhesion (oz/in.) | ASTM D-1000 | 50 - Acrylic; 30- Silicone |
| Tensile Strength (lb/in) | ASTM D3759 | 36 |
| Elongation (%) | ASTM D3759 | 165 |
| Dielectric Strength (volts) | ASTM D149 | 8800 |
| Max. Operating Temperature (°F) |  | 350F- Acrylic; 450F - Silicone |
| AVAILABILITY |  |  |
| Core I.D. (in) |  | 3 |
| Width (in) |  | .25 up to 24 |
| Roll Length (yd) |  | 36 |
| Release Liner |  | Kraft Paper- Acr; No Liner-Sil |

Note:  The above are “typical values” which have a nominal range about them and are not intended for specification purposes.

VICTREX PEEK® is a registered trademark of Victrex™, USA