Laminate Cross-Reference Chart & Governmental Agencies Specifications

| NEMA Grade | Military Spec. | Military Spec. Type | JAN-P-13 Type LTS | Navy 17-P-5 Type | Army 71-484 Type | ASTM (D-709) Type | MIL-I- 24768 | Federal Spec. L-L-31 (Formerly HHP-256) Type Grade | AAF Spec 12032 | Grade Description |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| - | - | PMB | M-1 | PBM | I | I | /12 | I | X | - | Paper Filler-Hard Phenolic Resin |
| X | MIL-P6885 (Formerly AN-P-68) | I (Cross Laminated) II (Parallel Laminated) | M-2 | PBM-1 | I | I | - | I | X | - |  |
| P XPC | - - | PMB-P PBM-PC | E-1 - | PBP - | - - | I-1 I | /19 /20 | I I | P PC | - - | Paper Filler- Plasticized Phenolic Resin Paper Filler- Elasticized Phenolic Resin |
| XX | MIL-P-3115 | PBG | E-2 | PBG | I | I | /11 | I | XX | - | Paper Filler-Hard Phenolic Resin |
| XXP | - | PBM-P | E-3 | - | - | I-2 | /21 | I | XXP | - | Paper Filler- Plasticized Phenolic Resin-For Hot Punching |
| XXX | MIL-P-3115 | PBE | E-4 | PBE | I | I-4 | /10 | I | XXX | - | Paper Filler-Hard Phenolic Resin |
| FR-2 |  | PBE-PCF |  |  |  |  | /25 |  |  |  | Paper Filler- Plasticized Phenolic Resin-For Hot Punching |
| XXXP | MIL-P-3115 | PBE-P | E-5 | PBE | - | I-3 | /22 | I | XXXP | - |  |
| XXXP-C |  |  |  |  |  |  | /23 |  |  |  |  |
| C | MIL-P-15035 MIL-P-55072* | FBM | M-4 | FBM | II | II | /16 | II | C | - | Medium Weight Cotton Fabric Filler-Hard Phenolic Resin |
| CE | MIL-P-15035 | FBG | EM-1 | FBG | II | II-5 | /14 | II | CE | - |  |
| - | MIL-P-5431 | - | - | - | - | - | - | - | - | CG | Medium Weight Cotton Fabric Filler-Hard Phenolic Resin With Graphite Inclusion |
| L | MIL-P-15035 | FBI | M-3 | FBI | II | II | /15 | II | L | - | Fine Weave Cotton Fabric Filler Hard Phenolic Resin |
| LE | MIL-P-15035 | FBE | EM-2 | FBE | II | II-5 | /13 | II | LE | - |  |
| - | MIL-P-5431 | - | - | - | - | - | - | - | - | LG | Fine Weave Cotton Fabric Filler-Hard Phenolic Resin With Graphite Inclusion |
| A | MIL-P-8059 (USAF) | PBA | H-1 | PBH | - | III | - | III | A | - | Asbestos Paper Filler- Hard Phenolic Resin |
| AA | MIL-P-8059 (USAF) | FBA | MH-1 | FBH | - | III | - | III | AA | - | Asbestos Paper Filler- Hard Phenolic Resin |
| - | - | - | M-5 | GBM GBH | - | IV | - | IV | - | - | Staple Fibre Glass Cloth Filler-Melamine Resin |
| G-3 | - | GPG | - | - | - | - | /18 | IV | G-3 | - | Glass Cloth Filler Phenolic Resin |
| G-5 G-7 | MIL-P-15037 MIL-P-997 | GMG GSG | MG-1 - | GMG GSG | - - | IV IV | /8 /17 | IV IV | G-5 G-7 | - - | Continuous Filament Glass Cloth Filler-Melamine Resin Continuous Filament Glass Cloth Filler-Silicone Resin |
| G-9 | MIL-P-15037 | GME | - | - | - | IV | /1 | IV | - | - | Glass Cloth Filler Melamine Resin |
| G-10 | MIL-P-18177 | GEE | - | - | - | IV | /2 | - | - | - | Continuous Filament Glass Cloth Filler-Epoxy Resin |
| G-11 FR-4 | MIL-P-18177 - | GEB GEE-F | - - | - - | - - | IV IV | /3 /27 | - IV | - - | - - | Continuous Filament Glass Cloth Filler-Epoxy Resin Glass Cloth Filler Epoxy FR Resin |
| FR-4 | - | GEB-F | - | - | - | IV | /28 | IV | - | - | Glass Cloth Filler Epoxy FR Resin |
| N-1 | MIL-P-15047 | NPG | - | - | - | V | /9 | V | N-1 | - | Nylon Fabric Filler-Phenolic Resin |
| - | MIL-P-14 | CFI-20 | - | - | III | - | - | III | - | - | Chopped Medium Weight Cotton Fabric-Hard Phenolic Resin |
| - | MIL-P-13949 | PP | - | - | - | - | - | - | - | - | Grade XXXP Copper Clad |
| CPF | MIL-P-8655 | - | - | - | - | - | - | - | - | - | Med. Weight Cotton Fabric Filler- Post Forming Phenolic Resin |
| FR-3 | MIL-P-22324 | PEE | - | - | - | - | /26 | - | - | - | Paper Filler-Flame Retardent Epoxy Resin |

Call Professional Plastics at (800) 966-7767 or

E-Mail sales@proplas.com

Order Online at www.professionalplastics.com