Pomalloy® ESd

Pomalloy ESd is a compound based on Acetal copolymer resin containing proprietary Anti-Static additives.

Plates and Rods are produced in standard and custom sizes upon request.

Standard Sheet Size: 24” x 48”  -   Thickness Range:  .250” up to 2.00”

Standard Rod Lengths: 10 feet  -   Standard Rod Diameters: .500” up to 3.00”

Property

| TYPICAL PROPERTIES (1) |
| --- |
| MECHANICAL | Value | Unit | Standard |  |
| Tensile Stress, yield | 420 | kgf/cm² | ASTM D 638 |  |
| Tensile Stress, break | 320 | kgf/cm² | ASTM D 638 |  |
| Tensile Strain, yield | 15.8 | % | ASTM D 638 |  |
| Tensile Strain, break | 59.5 | % | ASTM D 638 |  |
| Tensile Modulus, 50 mm/min | 16300 | kgf/cm² | ASTM D 638 |  |
| Flexural Stress | 490 | kgf/cm² | ASTM D 790 |  |
| Flexural Modulus | 14600 | kgf/cm² | ASTM D 790 |  |
| Tensile Stress, yield | 41 | MPa | ISO 527 |  |
| Tensile Stress, break | 36 | MPa | ISO 527 |  |
| Tensile Strain, yield | 13.3 | % | ISO 527 |  |
| Tensile Strain, break | 49.2 | % | ISO 527 |  |
| Tensile Modulus, 1 mm/min | 1500 | MPa | ISO 527 |  |
| Flexural Stress | 40 | MPa | ISO 178 |  |
| Flexural Modulus | 1500 | MPa | ISO 178 |  |
| IMPACT | Value | Unit | Standard |  |
| Izod Impact, unnotched, 23°C | NB | cm-kgf/cm | ASTM D 4812 |  |
| Izod Impact, notched, 23°C | NB | cm-kgf/cm | ASTM D 256 |  |
| Instrumented Impact Energy @ peak, 23°C | 293 | cm-kgf | ASTM D 3763 |  |
| Multiaxial Impact | 170 | cm-kgf | ISO 6603 |  |
| Izod Impact, unnotched 80*10*4 +23°C | NB | kJ/m² | ISO 180/1U |  |
| Izod Impact, notched 80*10*4 +23°C | 15 | kJ/m² | ISO 180/1A |  |
| THERMAL | Value | Unit | Standard |  |
| HDT, 0.45 MPa, 3.2 mm, unannealed | 146 | °C | ASTM D 648 |  |
| HDT, 1.82 MPa, 3.2mm, unannealed | 67 | °C | ASTM D 648 |  |
| CTE, -40°C to 40°C, flow | 1.3E-04 | 1/°C | ASTM E 831 |  |
| CTE, -40°C to 40°C, xflow | 1.33E-04 | 1/°C | ASTM E 831 |  |
| CTE, -40°C to 40°C, flow | 1.3E-04 | 1/°C | ISO 11359-2 |  |
| CTE, -40°C to 40°C, xflow | 1.33E-04 | 1/°C | ISO 11359-2 |  |
| PHYSICAL | Value | Unit | Standard |  |
| Density | 1.32 | g/cm³ | ASTM D 792 |  |
| Moisture Absorption, 50% RH, 24 hrs | 2.29 | % | ASTM D 570 |  |
| Mold Shrinkage, flow, 24 hrs | 1.8 | % | ASTM D 955 |  |
| Mold Shrinkage, xflow, 24 hrs | 1.8 | % | ASTM D 955 |  |
| Mold Shrinkage, flow, 24 hrs | 1.81 | % | ISO 294 |  |
| Mold Shrinkage, xflow, 24 hrs | 1.83 | % | ISO 294 |  |
| Wear Factor Washer | 14 | 10^-10 in^5-min/ft-lb-hr | ASTM D 3702 Modified |  |
| Dynamic COF | 0.42 | - | ASTM D 3702 Modified |  |
| Static COF | 0.25 | - | ASTM D 3702 Modified |  |
| Density | 1.33 | g/cm³ | ISO 1183 |  |
| Moisture Absorption (23°C / 50% RH) | 4.28 | % | ISO 62 |  |
| ELECTRICAL | Value | Unit | Standard |  |
| Surface Resistivity | 1.E+09 - 1.E+11 | Ohm | ASTM D 257 |  |

THESE PROPERTY VALUES ARE NOT INTENDED FOR SPECIFICATION PURPOSES.

(1) Typical values only. Variations within normal tolerances are possible for various colors. All values are measured after at least 48 hours storage at 23°C/50% relative humidity. All properties, except the melt volume and melt flow rates, are measured on injection molded samples. All samples tested under ISO test standards are prepared according to ISO 294.

(2) Only typical data for selection purposes. Not to be used for part or tool design.

(3) This rating is not intended to reflect hazards presented by this or any other material under actual fire conditions.

(4) Internal measurements according to UL standards.
Disclaimer : ALTHOUGH ANY INFORMATION, RECOMMENDATIONS, OR ADVICE CONTAINED HEREIN IS GIVEN IN GOOD FAITH, PROFESSIONAL PLASTICS  MAKES NO WARRANTY OR GUARANTEE, EXPRESS OR IMPLIED, (I) THAT THE RESULTS DESCRIBED HEREIN WILL BE OBTAINED UNDER END-USE CONDITIONS, OR (II) AS TO THE EFFECTIVENESS OR SAFETY OF ANY DESIGN INCORPORATING MATERIALS, PRODUCTS, RECOMMENDATIONS OR ADVICE. EXCEPT AS PROVIDED IN PROFESSIONAL PLASTICS STANDARD CONDITIONS OF SALE, PROFESSIONAL PLASTICS AND ITS REPRESENTATIVES SHALL IN NO EVENT BE RESPONSIBLE FOR ANY LOSS RESULTING FROM ANY USE OF ITS MATERIALS OR PRODUCTS DESCRIBED HEREIN. Each user bears full responsibility for making its own determination as to the suitability of materials, products, recommendations, or advice for its own particular use. Each user must identify and perform all tests and analyses necessary to assure that its finished parts incorporating materials or products will be safe and suitable for use under end-use conditions. Nothing in this or any other document, nor any oral recommendation or advice, shall be deemed to alter, vary, supersede, or waive any provision of Professional Plastics Conditions of Sale or this Disclaimer, unless any such modification is specifically agreed to in a writing signed by Professional Plastics. No statement contained herein concerning a possible or suggested use of any material, product or design is intended, or should be construed, to grant any license under any patent or other intellectual property right of Professional Plastics or any of its subsidiaries or affiliates covering such use or design, or as a recommendation for the use of such material, product or design in the infringement of any patent or other intellectual property right.

- Pomalloy ESd is a trademark of Professional Plastics, Inc.  Any unauthorized use of this trade name is strictly prohibited.  Pomalloy ESd is exclusively supplied by Professional Plastics, Inc.

PROFESSIONAL PLASTICS, INC.

Toll-Free USA (800) 966-7767

www.professionalplastics.com

E-Mail: sales@proplas.com