Radel® R PPSU, Polyphenylsulfone, unfilled, extruded
Search Categories: Polyphenylsulfone; ; FDA Approved

Material Notes: Radel* R is an extruded form of polyphenylsulfone (PPSU) that offers higher impact resistance and has superior hydrolysis resistance than other amorphous materials, including both polysulfone and polyetherimide (PEI). It retains much of the thermal resistance, stability, and machinability of PEI. These properties make it ideal for medical applications requiring autoclaving.

| MECHANICAL PROPERTIES | ENGLISH VALUES | COMMENTS | METRIC VALUES |
| --- | --- | --- | --- |
| Specific Gravity | 1.29 | ASTM D792 | 1.29 |
| Tensile Strength, psi | 11000 | ASTM D638 | 76 MPa |
| Tensile Modulus, psi | 340000 | ASTM D638 | 2,344 MPa |
| Elongation, % | 30 | ASTM D638 | 30 % |
| Flexural Strength, psi | 15500 | ASTM D790 | 107 MPa |
| Flexural Modulus, psi | 345000 | ASTM D790 | 2,379 MPa |
| Shear Strength, psi | 9000 | ASTM D732 | 62 MPa |
| Compressive Strength, psi | 13400 | ASTM D695, 10% Def. | 92 MPa |
| Compressive Modulus, psi | 280000 | ASTM D695 | 1,931 MPa |
| Hardness, Rockwell M | 80 | ASTM D785 | 80 |
| Hardness, Rockwell R | 120 | ASTM D785 | 120 |
| Hardness, Durometer, Shore D Scale | 80 | ASTM D2240 | 80 |
| Izod Impact (Notched), ft-lb/in | 2.5 | ASTM D256 Type A | 133 J/m |
| Limiting PV, psi-fpm | 1000 | PTM55007 | 0.04 MPa-m/sec |
| k (wear) factor, 10-10in3-min/lb-ft-hr | 1000 | PTM55007 | 1000 10-10in3-min/lb-ft-hr |
| THERMAL PROPERTIES | ENGLISH VALUES | COMMENTS | METRIC VALUES |
| Coefficient of Thermal Expansion, 10E-4/°F | 0.31 | ASTM E831 (TMA) | 0.56 10-4/K |
| Deflection Temperature 264 psi, ºF | 405 | ASTM D648 | 207 °C |
| Tg-Glass Transition (Amorphous), ºF | 428 | ASTM D3418 | 220 °C |
| Continuous Service in Air (Max), °F | 300 | Without Load | 149 °C |
| Thermal Conductivity, BTU-in/hr-ft²-°F | 2.4 |  | 0.35 W/m-K |
| ELECTRICAL PROPERTIES | VALUES | COMMENTS | METRIC VALUES |
| Dielectric Strength, Short Term, Volts/mil | 360 | ASTM D149(2) | 14 kV/mm |
| Surface Resistance, Ohm/Square | 1E+13 | Lower Limit; EOS/ESD S11.11 | 1E+13 Ohm/Square |
| Dielectric Constant, 1 MHz | 3.44 | ASTM D150(2) | 3.44 |
| Dissipation Factor, 1 MHz | 0.0017 | ASTM D150(2) | 0.0017 |
| CHEMICAL PROPERTIES | ENGLISH VALUES | COMMENTS | METRIC VALUES |
| Water Absorption Immersion, 24 hr., % | 0.37 | ASTM D570 | 0.37 % |
| Water Absorption Immersion Sat, % | 1.1 | ASTM D570 | 1.1 % |
| Acids, Weak (acetic, dilute HCl) | 3 | Acceptable Service | 3 |
| Acids, Strong (conc. HCl or sulfuric) | 2 | Limited Service | 2 |
| Alkalies, Weak (dilute NaOH) | 3 | Acceptable Service | 3 |
| Alkalies, Strong (conc. NaOH) | 3 | Acceptable Service | 3 |
| Hydrocarbons, Aromatic (toluene) | 2 | Limited Service | 2 |
| Hydrocarbons, Aliphatic (gasoline) | 3 | Acceptable Service | 3 |
| Ketones, Esters (acetone) | 1 | Unnacceptable | 1 |
| Ethers (diethyl ether, THF) | 2 | Limited Service | 2 |
| Chlorinated Solvents (methylene chloride) | 1 | Unnacceptable | 1 |
| Alcohols (methanol, anti-freeze) | 2 | Limited Service | 2 |
| Inorganic Salt Solutions (NaCl, KCl) | 3 | Acceptable Service | 3 |
| Continuous Sunlight | 2 | Limited Service | 2 |
| Steam | 3 | Acceptable Service | 3 |
| COMPLIANCE | ENGLISH VALUES | COMMENTS | METRIC VALUES |
| Flammability, UL94 (5=V-0; 4=V-1; 3=V-2; 1=HB) | 5 (V-0) | UL94 | 5 |
| FDA (1=Yes) | 1 | Compliant | 1 |
| USDA (1=Yes) | 0 | Not Compliant | 0 |
| NSF (1=Yes) | 0 | Not Compliant | 0 |
| 3A-Dairy (1=Yes) | 0 | Not Compliant | 0 |
| Canada AG (1=Yes) | 1 | Compliant | 1 |
| USP Class VI (1=Yes) | 1 | Compliant | 1 |