Ryton® PPS 40% GF (CM), Polyphenylene sulfide, 40% glass reinforced, compression molded
Search Categories: Polyphenylene Sulfide; ;

Material Notes: Compression molded 40% glass fiber reinforced Ryton polyphenylene sulfide. PPS products offer the broadest resistance to chemical of any advanced engineering plastic. This grade offers better dimensional stability and thermal performance than Techtron PPS and maintains its strength to above 425°F.

| MECHANICAL PROPERTIES | ENGLISH VALUES | COMMENTS | METRIC VALUES |
| --- | --- | --- | --- |
| Specific Gravity | 1.7 | ASTM D792 | 1.7 |
| Tensile Strength, psi | 13000 | ASTM D638 | 90 MPa |
| Tensile Modulus, psi | 730000 | ASTM D638 | 5,033 MPa |
| Elongation, % | 2 | ASTM D638 | 2 % |
| Flexural Strength, psi | 23000 | ASTM D790 | 159 MPa |
| Flexural Modulus, psi | 1000000 | ASTM D790 | 6,895 MPa |
| Compressive Strength, psi | 24000 | ASTM D695, 10% Def. | 165 MPa |
| Compressive Modulus, psi | 1300000 | ASTM D695 | 8,964 MPa |
| Hardness, Rockwell M | 94 | ASTM D785 | 94 |
| Hardness, Rockwell R | 125 | ASTM D785 | 125 |
| Hardness, Durometer, Shore D Scale | 86 | ASTM D2240 | 86 |
| Izod Impact (Notched), ft-lb/in | 1 | ASTM D256 Type A | 53 J/m |
| Limiting PV, psi-fpm | 3500 | PTM55007 | 0.12 MPa-m/sec |
| THERMAL PROPERTIES | ENGLISH VALUES | COMMENTS | METRIC VALUES |
| Coefficient of Thermal Expansion, 10E-4/°F | 0.25 | ASTM E831 (TMA) | 0.45 10-4/K |
| Deflection Temperature 264 psi, ºF | 490 | ASTM D648 | 254 °C |
| Melting Point (Crystalline) Peak, °F | 540 | ASTM D3418 | 282 °C |
| Continuous Service in Air (Max), °F | 450 | Without Load | 232 °C |
| Thermal Conductivity, BTU-in/hr-ft²-°F | 2.1 |  | 0.30 W/m-K |
| ELECTRICAL PROPERTIES | VALUES | COMMENTS | METRIC VALUES |
| Dielectric Strength, Short Term, Volts/mil | 385 | ASTM D149(2) | 15 kV/mm |
| Surface Resistance, Ohm/Square | 1E+13 | Lower Limit; EOS/ESD S11.11 | 1E+13 Ohm/Square |
| CHEMICAL PROPERTIES | ENGLISH VALUES | COMMENTS | METRIC VALUES |
| Water Absorption Immersion, 24 hr., % | 0.02 | ASTM D570 | 0.02 % |
| Water Absorption Immersion Sat, % | 0.03 | ASTM D570 | 0.03 % |
| Acids, Weak (acetic, dilute HCl) | 3 | Acceptable Service | 3 |
| Acids, Strong (conc. HCl or sulfuric) | 2 | Limited Service | 2 |
| Alkalies, Weak (dilute NaOH) | 3 | Acceptable Service | 3 |
| Alkalies, Strong (conc. NaOH) | 3 | Acceptable Service | 3 |
| Hydrocarbons, Aromatic (toluene) | 3 | Acceptable Service | 3 |
| Hydrocarbons, Aliphatic (gasoline) | 3 | Acceptable Service | 3 |
| Ketones, Esters (acetone) | 3 | Acceptable Service | 3 |
| Ethers (diethyl ether, THF) | 3 | Acceptable Service | 3 |
| Chlorinated Solvents (methylene chloride) | 3 | Acceptable Service | 3 |
| Alcohols (methanol, anti-freeze) | 3 | Acceptable Service | 3 |
| Inorganic Salt Solutions (NaCl, KCl) | 3 | Acceptable Service | 3 |
| Continuous Sunlight | 2 | Limited Service | 2 |
| Steam | 3 | Acceptable Service | 3 |
| COMPLIANCE | ENGLISH VALUES | COMMENTS | METRIC VALUES |
| Flammability, UL94 (5=V-0; 4=V-1; 3=V-2; 1=HB) | 5 (V-0) | UL94 | 5 |
| FDA (1=Yes) | 0 | Not Compliant | 0 |
| USDA (1=Yes) | 0 | Not Compliant | 0 |
| NSF (1=Yes) | 0 | Not Compliant | 0 |
| 3A-Dairy (1=Yes) | 0 | Not Compliant | 0 |
| Canada AG (1=Yes) | 0 | Not Compliant | 0 |
| USP Class VI (1=Yes) | 0 | Not Compliant | 0 |