Spirally Cut Tubing: Polyethylene

Polyethylene is ideal for general applications, this low-cost material is highly abrasion resistant and is not affected by most solvents. Also available in Ultraviolet-Resistant Black (for outdoor use), and many colors.

| Size |  | Outside Diameter O.D. | Nominal Dimensions Wall | Inside Diameter I.D. | Pitch | Maximum Bundle Range Inches | Weight Lbs/M Ft. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Natural Polyethylene |
| 1/8" |  | 0.125 | 0.032 | 0.061 | 0.187 | 1/16 to 1/2 | 4 |
| 3/16" |  | 0.187 | 0.030 | 0.127 | 0.250 | 1/8 to 1 1/2 | 6 |
| 1/4" |  | 0.250 | 0.035 | 0.180 | 0.375 | 3/16 to 2 | 9 |
| 1/4" |  | 0.250 | 0.045 | 0.160 | 0.375 | 3/16 to 2 | 12 |
| 3/8" |  | 0.375 | 0.052 | 0.271 | 0.438 | 5/16 to 3 | 22 |
| 1/2" |  | 0.500 | 0.040 | 0.420 | 0.563 | 3/8 to 4 | 26 |
| 1/2" |  | 0.500 | 0.062 | 0.375 | 0.563 | 3/8 to 4 | 35 |
| 5/8" |  | 0.625 | 0.062 | 0.500 | 0.625 | 1/2 to 4 1/2 | 44 |
| 3/4" |  | 0.750 | 0.065 | 0.620 | 0.750 | 3/4 to 5 | 58 |
| 1" |  | 1.000 | 0.080 | 0.840 | 1.000 | 1 to 7 | 105 |
| 1 1/4" |  | 1.250 | 0.090 | 1.070 | 1.250 | 1 1/4 to 8 | 190 |
| 1 1/2" |  | 1.500 | 0.100 | 1.300 | 1.500 | 1 1/2 to 10 | 178 |
| Ultraviolet-Resistant Black Polyethylene |
| 1/8" |  | 0.125 | 0.032 | 0.061 | 0.187 | 1/16 to 1/2 | 4 |
| 3/16" |  | 0.187 | 0.030 | 0.127 | 0.250 | 1/8 to 1 1/3 | 6 |
| 1/4" |  | 0.250 | 0.035 | 0.180 | 0.375 | 3/16 to 2 | 9 |
| 1/4" |  | 0.250 | 0.045 | 0.160 | 0.375 | 3/16 to 2 | 12 |
| 3/8" |  | 0.375 | 0.052 | 0.271 | 0.438 | 5/16 to 3 | 22 |
| 1/2" |  | 0.500 | 0.040 | 0.420 | 0.563 | 3/8 to 4 | 26 |
| 1/2" |  | 0.500 | 0.062 | 0.375 | 0.563 | 3/8 to 4 | 35 |
| 5/8" |  | 0.625 | 0.062 | 0.500 | 0.625 | 1/2 to 4 1/2 | 44 |
| 3/4" |  | 0.750 | 0.065 | 0.620 | 0.750 | 3/4 to 5 | 58 |
| 1" |  | 1.000 | 0.080 | 0.840 | 1.000 | 1 to 7 | 105 |
| 1 1/4" |  | 1.250 | 0.090 | 1.070 | 1.250 | 1 1/4 to 8 | 190 |
| 1 1/2" |  | 1.500 | 0.100 | 1.300 | 1.500 | 1 1/2 to 10 | 178 |

Properties of Polyethylene

| Max-Min Oper Temp | Abrasion Resistence | Specific Gravity D792-66 | Effect of Solvents | Effect of Acids | Effect of Alkalies | Water Absorption % D-570 | Flammability | MIL Spec. & Approvals |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Natural Polyethylene |
| 190°F 88°C | -76°F -60°C | 22 | 0.92 | None below 122°F 50°C | None | None | .014 | Flammable | Fed. Spec. LP390 MIL I-631D MIL P-21922A |
| Ultraviolet-Resistant Black Polyethylene |
| 190°F 88°C | -76°F -60°C | 20 | 0.93 | None below 122°F 50°C | None | None | .03 | Flammable | Fed. Spec. LP390 MIL I-631D MIL P-21922A |