Spirally Cut Tubing: TFE

TFE is suitable for the widest operating temperature range of any material and can be used from -450° F to +500° F. Chemically inert and non-flammable, it is also available in black and a wide selection of colors.

| Size | Part No. | Outside Diameter O.D. | Nominal Dimensions Wall | Inside Diameter I.D. | Pitch | Maximum Bundle Range Inches | Weight Lbs/M Ft. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| TFE (available in black and a wide selection of colors) |
| 1/16" |  | 0.062 | 0.016 | 0.030 | 0.062 | 1/32 to 1/8 | 4.2 |
| 1/8" |  | 0.125 | 0.030 | 0.065 | 0.187 | 1/16 to 1/2 | 9.4 |
| 1/8" | HT 1/8T2-Thin Wall | 0.125 | 0.020 | 0.085 | 0.187 | 1/16 to 1/2 | 7.4 |
| 3/16" |  | 0.187 | 0.030 | 0.127 | 0.250 | 1/8 to 1 1/2 | 15.2 |
| 1/4" |  | 0.250 | 0.030 | 0.187 | 0.375 | 3/16 to 2 | 20.7 |
| 3/8" |  | 0.375 | 0.030 | 0.312 | 0.438 | 5/16 to 2 1/2 | 36.5 |
| 1/2" |  | 0.500 | 0.030 | 0.438 | 0.500 | 3/8 to 3 | 50.5 |
| 5/8" |  | 0.625 | 0.030 | 0.565 | 0.625 | 5/8 to 3 1/2 | 65.5 |
| 3/4" |  | 0.750 | 0.032 | 0.686 | 0.750 | 1/2 to 4 | 81.3 |
| 1" |  | 1.000 | 0.040 | 0.920 | 1.000 | 3/4 to 5 | 175.0 |

Properties of TFE

| Max-Min Oper Temp | Abrasion Resistance | Specific Gravity D792-66 | Effect of Solvents | Effect of Acids | Effect of Alkalies | Water Absorption % D-570 | Flammability | MIL Spec. & Approvals |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| TFE |
| 500°F 260°C | -450°F -268°C | 7 | 2.1 | None | None | None | 0.05 | Non-flammable | AMS 365 1C AMS 3653C AMS 3654 AMS 3655 ASTM D3295 MIL I-22129C P-22296B MIL T-47287A Type I AS 1294 |