| Typical Properties of TPX ® PolyMethylPentene |
| --- |
| ASTM or UL test | Property | TPX |
| PHYSICAL |
| D792 | Density (lb/in³) (g/cm³) | 0.030 0.83 |
| D570 | Water Absorption, 24 hrs (%) | 0.01 |
| MECHANICAL |
| D638 | Tensile Strength (psi) | 4,100 |
| D638 | Tensile Modulus (psi) | 280,000 |
| D638 | Tensile Elongation at Break (%) | 10 |
| D790 | Flexural Strength (psi) | 6,100 |
| D790 | Flexural Modulus (psi) | 210,000 |
| D695 | Compressive Strength (psi) | - |
| D695 | Compressive Modulus (psi) | - |
| D785 | Hardness, Shore D | D85 |
| D256 | IZOD Notched Impact (ft-lb/in) | 1 |
| THERMAL |
| D696 | Coefficient of Linear Thermal Expansion (x 10-5 in./in.- °F) | 6.5 |
| D648 | Heat Deflection Temp (°F / °C) at 264 psi | 212 / 100 |
| D3418 | Melting Temp (°F / °C) | 464 / 240 |
| - | Max Operating Temp (°F / °C) | - / - |
| C177 | Thermal Conductivity (BTU-in/ft²-hr-°F) (x 10-4 cal/cm-sec-°C) | 1.16 4.0 |
| UL94 | Flammability Rating | HB |
| ELECTRICAL |
| D149 | Dielectric Strength (V/mil) short time, 1/8" thick | 20 |
| D150 | Dielectric Constant at 1 KHz | 2.12 |
| D150 | Dissipation Factor at 1 MHz | 0.000025 |
| D257 | Volume Resistivity (ohm-cm)at 50% RH | > 1016 |

All values at 73°F (23°C) unless otherwise noted.

Note: The information contained herein are typical values intended for reference and comparison purposes only. This data should not be used as the sole basis for design specifications or quality control.

TPX is a registered trademark of Mitsui Petrochemical Industries, Ltd.