| TEXfluor® FEP 1.3/1 Heat Shrinkable Tubing |
| --- |
| Generally, the FEP 1.3/1 Heat Shrinkable Tubing grows in length upon shrinking. Allow the FEP shrink to slide forward to prevent Wrinkling. |
| FEP 1.3/1 AWG HEAT SHRINK SIZES |
| AWG SIZE | INSIDE DIAMETER | RECOVERED WALL THICKNESS | APPX. WEIGHT | M23053/11 |
|  | MIN EXPANDED I.D. | MAX RECOVERED I.D. |  |  |  |
|  | INCH | MM | INCH | MM | INCHES +or- | MM +or- | LB/FT | KG/M |  |
| 24 22 20 | .031 .036 .045 | .787 .914 1.14 | .027 .032 .039 | .686 .813 .991 | .008 .002 .008 .002 .008 .002 | .203 .051 .203 .051 .203 .051 | .0015 .0016 .0023 | .0022 .0024 .0034 | 101 102 103 |
| 18 16 14 | .060 .075 .092 | 1.52 1.91 2.34 | .049 .061 .072 | 1.25 1.55 1.83 | .008 .002 .009 .002 .009 .002 | .203 .051 .229 .051 .229 .051 | .0027 .0030 .0031 | .0040 .0045 .0046 | 104 105 106 |
| 12 10 9 | .115 .141 .158 | 2.92 3.58 4.01 | .089 .114 .124 | 2.26 2.90 3.15 | .009 .002 .010 .003 .010 .003 | .229 .051 .254 .076 .254 .076 | .0032 .0039 .0043 | .0048 .0058 .0064 | 107 108 109 |
| 8 7 6 | .180 .197 .225 | 4.57 5.00 5.72 | .143 .158 .180 | 3.63 4.01 4.57 | .010 .003 .011 .004 .011 .004 | .254 .076 .279 .102 .279 .102 | .0048 .0068 .0076 | .0071 .0101 .0113 | 110 111 112 |
| 5 4 3 | .248 .290 .310 | 6.30 7.37 7.87 | .198 .226 .249 | 5.03 5.74 6.32 | .011 .004 .011 .004 .011 .004 | .279 .102 .279 .102 .279 .102 | .0084 .0094 .0105 | .0125 .0140 .0156 | 113 114 115 |
| 2 1 0 | .365 .400 .440 | 9.27 10.2 11.2 | .280 .311 .349 | 7.11 7.90 8.86 | .012 .004 .012 .004 .012 .004 | .305 .102 .305 .102 .305 .102 | .0117 .0132 .0180 | .0174 .0196 .0268 | 116 117 118 |
| FEP 1.3/1 FRACTIONAL HEAT SHRINK SIZES |
| 3/8 7/16 1/2 | .500 .580 .666 | 12.7 14.7 16.9 | .383 .448 .510 | 9.73 11.4 13.0 | .015 .004 .020 .004 .020 .004 | .381 .102 .508 .102 .508 .102 | .0233 .0366 .0400 | .0347 .0545 .0595 | 119 120 121 |
| 5/8 3/4 7/8 | .830 1.00 1.17 | 21.1 25.4 29.7 | .637 .764 .891 | 16.2 19.4 22.6 | .025 .004 .030 .004 .035 .004 | .635 .102 .762 .102 .889 .102 | .0631 .0929 .1266 | .0939 .1382 .1884 | 122 123 124 |
| 1 1-1/8 1-1/4 | 1.33 1.50 1.67 | 33.8 38.1 42.3 | 1.02 1.15 1.27 | 25.9 29.1 32.3 | .035 .004 .035 .004 .035 .004 | .889 .102 .889 .102 .889 .102 | .1439 .1900 .2250 | .2141 .2827 .3348 | 126 - - |
| 1-3/8 1-1/2 | 1.83 2.00 | 46.6 50.8 | 1.39 1.52 | 35.3 38.6 | .035 .004 .035 .004 | .889 .102 .889 .102 | .2750 .2890 | .4092 .4300 | - 127 |
| Meets Specifications: | AMS-DTL-23053/11 1** FEP 1.3/1 HEAT SHRINK ASTM D2902 TYPE II |
| FEP Shrink Temperature: | 1" dia. and below: 410°F / 210°C Over 1" dia.: 430°F / 221°C |
| FEP Continuous Use Temperature Range: | -100 to 400°F -75 to 200°C |
| Dielectric Strength: | > 2,000 V/M* |
| Longitudinal Change: | + 15% |
| Color: | Translucent |
| Standard Shipping Lengths: | 4 ft and coils |
| * Per ASTM D 149 Short Term Test of 10 MIL Thickness (Volts/Mil) |