| TEXfluor® FEP 1.67/1 Heat Shrinkable Tubing |
| --- |
| FEP 1.67/1 Heat Shrinkable Tubing is available in custom sizes and colors. We also offer tube scoring, cutting, kits, custom shrinking and more. |
| FRAC SIZE | INSIDE DIAMETER | RECOVERED WALL THICKNESS | APPX. WEIGHT | M23053/11 |
|  | MIN EXPANDED I.D. | MAX RECOVERED I.D. |  |  |  |
|  | INCH | MM | INCH | MM | INCHES +or- | MM +or- | LB/FT | KG/M |  |
| 3/32 1/8 3/16 | .093 .125 .188 | 2.36 3.18 4.78 | .056 .075 .115 | 1.42 1.91 2.92 | .008 .003 .010 .003 .010 .003 | .203 .076 .254 .076 .254 .076 | .0045 .0046 .0058 | .0066 .0068 .0086 | 201 202 203 |
| 1/4 3/8 1/2 | .250 .375 .500 | 6.35 9.53 12.7 | .150 .225 .300 | 3.81 5.72 7.62 | .010 .003 .012 .003 .015 .004 | .254 .076 .305 .076 .381 .102 | .0086 .0140 .0283 | .0127 .0207 .0418 | 204 205 206 |
| 3/4 1 1-1/2 2 | .750 1.00 1.50 2.00 | 19.0 25.4 38.1 50.8 | .450 .600 .900 1.20 | 11.43 15.24 22.86 30.48 | .020 .004 .025 .005 .030 .005 .030 .005 | .508 .102 .635 .127 .762 .127 .762 .127 | .0540 .0639 .1260 .2200 | .0797 .0943 .1860 .3248 | 207 208 209 210 |
| Meets Specifications: | AMS-DTL-23053/11 2** FEP 1.67/1 HEAT SHRINK ASTM D2902 TYPE II |
| FEP Shrink Temperature: | 1" dia. and below: 410°F / 210°C Over 1" dia.: 430°F / 221°C |
| FEP Continuous Use Temperature Range: | -100 to 400°F -75 to 200°C |
| Dielectric Strength: | > 2,000 V/M* |
| Longitudinal Change: | + 15% |
| Color: | Translucent |
| Standard Shipping Lengths: | 4 ft and coils |
| * Per ASTM D 149 Short Term Test of 10 MIL Thickness (Volts/Mil) |