KYNStick Kynar® Tape with Pressure Sensitive Adhesive

PRODUCT DESCRIPTION

KYNStick® Tape offers excellent chemical and corrosion resistance and has a high tensile strength. KYNStick® has good thermal stability and can be used in applications up to 300°F. Kynar® has extremely high purity which makes it a good candidate for food applications. When specified, Kynar 740 FILM complies with FDA regulation 21 CFR 177.510, USDA, USP XX Class VI, 3A sanitary standards and meets ASTM D3222 resin specifications. KYNStick® Tape also possesses high impact resistance and is tough and durable. KynStick® is Clear with a Peel-off liner. Kynar can be used as a substitute for Tedlar®- ask for info.

ADHESIVE INFORMATION

For general purposes, Acrylic Adhesive offers good adhesion, chemical and environmental resistance.

TECHNICAL DATA

PROPERTY DATA Backing Material Kynar Film Backing Thickness (in) .005" or .010" Adhesive System Acrylic Adhesive Thickness (in.) .002” or .005" Tensile Strength (pli) 31.08 Elongation (%) 45.1 Dielectric Breakthrough (kV) 7.52 Peel Strength (pli) 3.53 Max. Operating Temp. (F) 300 AVAILABILITY Core Dia. (in) 3" Width (in.) .125-36 Roll Length 36 – 60 yds

Call Professional Plastics at (800) 966-7767 or

E-Mail sales@proplas.com

Order Online at www.professionalplastics.com