##### Spartech SP-9010 General Purpose ABS Sheet

Subcategory: ABS Polymer; Polymer; Thermoplastic

Material Notes: 
Description: ABS Sheet

Information provided by Spartech.

| Physical Properties | Metric | English | Comments |
| --- | --- | --- | --- |
| Specific Gravity | 1.04 g/cc | 0.0376 lb/in³ | ASTM D792 |
| Mechanical Properties |
| Hardness, Rockwell R | 105 | 105 | ASTM D785 |
| Tensile Strength @ Yield | 41.4 MPa | 6000 psi | ASTM D638 |
| Tensile Modulus | 2.14 GPa | 310 ksi | ASTM D638 |
| Flexural Modulus | 2.34 GPa | 340 ksi | ASTM D790 |
| Flexural Yield Strength | 68.9 MPa | 10000 psi | ASTM D790 |
| Izod Impact, Unnotched | 4 J/cm | 7.5 ft-lb/in | ASTM D256 |
| Falling Dart Impact | 16.3 J | 12 ft-lb | -40°F; ASTM D3029 |
| Falling Dart Impact | 44.7 J | 33 ft-lb | 73°F; ASTM D3029 |
| Izod Impact, Unnotched @ -40°C | 1.33 J/cm | 2.5 ft-lb/in | ASTM D256 |
| Thermal Properties |
| CTE, linear 68°F | 90 µm/m-°C | 50 µin/in-°F | ASTM D696 |
| Deflection Temperature at 1.8 MPa (264 psi) | 92.2 °C | 198 °F | ASTM D648 |
| Flammability, UL94 | HB | HB |  |
| Optical Properties |
| Gloss | 90 % | 90 % | Gardner; ASTM D2523 |
| Descriptive Properties |
| Flammability | Passes | MVSS (Motor Vehicle Safety Standard) 302 |

# Text boxes

Need help with your order? Call us at 1-800-966-PROS 
or order online at www.professionalplastics.com today!