Arboron ® Technical Data Sheet

| PHYSICAL PROPERTIES |
| --- |
| Density Specific Gravity |  | 86.4 lbs/ft3 (1 384 kg/m3) 1.39 gm/c3 | Rockwell Hardness ASTM D 785-89 | M scale |
| Tensile Strength ASTM D 638 | M.D. C.D. | 22,000 psi (151,865 kPa) 16,000 psi (110,316 kPa) | Water Absorption ASTM D 570-63e | 1/8''(3.2 mm) |
| Flexural Strength ASTM D 790-86 | M.D. C.D. | 23,000 psi (158,579 kPa) 15,000 psi (103,421 kPa) | Thickness Tolerance | in accordance with NEMA standards L¦1 1989 |
| Compressive Strength ASTM D 695-89 | Flatwise Edgewise | 22,700 psi (156,511 kPa) 43,600 psi (300,611 kPa) | Wrap or Twist Tolerances | in accordance with NEMA standards L¦1 1989 |
| Elastic Modulus ASTM D 790-89 | M.D. C.D. | 2,370,000 psi (16.3 M kPa) 1,780,000 psi (12.3 M kPa) | Oil Compatibility Arboron shows no adverse effects on electrical insulating oil/transformer, as per ASTM D3455 test method. |
| Impact Strength Edgewise | M.D. C.D. | 0.6 ft lbs/in 0.5 ft lbs/in | Material Safety Data Sheet | MSDS Code Conlam 0036 |
| Bond Strength ASTM D 229-86 |  | 659 psi |  |  |

| ELECTRICAL PROPERTIES Arboron® can easily be fabricated using carbide tipped, standard machine tools for sawing, drilling and tapping, milling, turning and routing. | Relative Thermal Index 95°C Electrical and Mechanical ASTM D 790 U.L. 94 Flame Classification Flame spread left <20:smoke development<70 0.061" (1.6 mm) 94 HB 0.240" (6.1 mm) 94 VO Arc Resistance (dry) 135 sec ASTM D 495-89 |
| --- | --- |
|  | Dielectric Strength ASTM D 229, Condition A |  |  |
|  |  | S/S | S/T |
|  |  | (step by step) | (short time) |
|  | Parallel to Laminations |  |  |
|  | 1/4" (6.4 mm) | 48 kV | 66kV |
|  | 1/2" (12.7 mm) | 40 kV | 50kV |
|  | 1"(25.4 mm) | 36kV | 42kV |
|  | Perpendicular to Laminations |  |  |
|  | volts/mil 1/4"(6.4 mm) | 200 | 250 |
|  | 1/2"(12.7 mm) | 120 | 150 |
|  | 1"(25.4 mm) | 85 | 100 |
|  | Dissipation Factor 1/4" (6.4 mm) 0.0481 ASTM D 150-92 Dielectric Constant 1/4"(6.4 mm) 5.41 Insulation Resistance (C/96/35/90) 500 megohms Surface Resistance (C/96/35/90 200 megohms Volume Resistivity (C/96/35/90) 22 megohms (condition of the three listed above=C96 hr/35 C90% R.H.) Comparative Track Index (CTI) 600V High Ampere Arc Ignition (HAI) 200 + Hot Wire Ignition (HWI) 107 sec |

# Text boxes

Need help with your order? Call us at 1-800-966-PROS 
or order online at www.professionalplastics.com today!

See Arboron ® Electrical Properties Below