Ceramic – Comparative Material Data Sheets

|  | Properties | Units | Test | 99.5% Alumina | Aluminum Nitride | Boron Nitride | Lava, Grade A | Corning Macor® | Mullite | Silicon Carbide | Silicon Nitride (Hot Pressed) | Steatite L-5 | Zirconia |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Chemical Formula | - | - | Al2O3 | AlN | BN | Al2(Si4010)(OH)2 | glass ceramic | 3Al203-SiO2 | -SiC | Si3N4 | H2Mg3(SiO3)4 | ZrO2 |
|  | Density | g/cm3 | ASTM C20 | 3.7 - 3.97 | 3.25 | 2.28 | 2.30 | 2.52 | 2.80 | 3.21 | 3.31 | 2.71 | 6.04 |
|  | Color | - | - | ivory/white | white/tan/gray | white | pink | white | tan | dark gray | dark gray | buff | white |
|  | Crystal Structure | - | - | hexagonal | hexagonal | hexagonal | random | random | orthorhombic | hexagonal | hexagonal ( & ) | hexagonal | tetragonal |
|  | Water Absorption | % @ R.T. | ASTM C373 | 0.0 | 0.0 | 0.0-1.0 | 2.5 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0-0.02 | 0.0 |
|  | Hardness | Moh's | - | 9 | 5 | 2 | 6 | 4.5 | 8 | 10-Sep | 9 | 7.5 | 6.5 |
|  | Hardness | knoop(kg/mm1) | Knoop 100g | 2000 | 1170 | 25-205 | 500 | 250 | 1450 | 2800 | 2200 | - | 1600 |
|  | Compressive Strength | MPa @ R.T. | ASTM C773 | 2070-2620 | 2068 | 23.5 | 172.5 | 345 | 551 | 1725-2500 | 689-2760 | 621 | 2500 |
|  | Tensile Strength | MPa @ R.T. | ACMA Test #4 | 260-300 | - | 2.41 (1000¡C) | 20.7 | 90 | 103.5 | 310 | 360-434 | 62 | 248 |
|  | Modulus of Elasticity (Young'sMod.) | GPa | ASTM C848 | 394 | 308 | 675 | - | 66.9 | 150 | 476 | 317 | 138 | 207 |
|  | Flexural Strength (MOR) | MPa @ R.T. | ASTM F417 | 310-379 | 428 | 51.8 | 69 | 94 | 170 | 324 | 679-896 | 140 | 900 |
|  | Poisson's Ratio | - | ASTM C818 | 0.27 | 0.25 | 0.05 | - | 0.29 | 0.25 | 0.19 | 0.23 | - | 0.32 |
|  | Fracture Toughness | Mpa x m1/2 | Notched Beam Test | 4.50 | 3.50 | 2.60 | - | 1.53 | 2.00 | 4.0 | 5.0-8.0 | - | 13.0 |
|  | Max. Use Temperature (*denotes inert atm.) | ¡C | No load cond. | 1750 | 1600 | 985 | 1150 | 1000 | 1700 | 1400 | 1500 | 1425 | 500 |
|  | Thermal Shock Resistance | T (¡C) | Quenching | 200 | 400 | >1500 | - | 25-100 | 300 | 350-500 | 750 | 190 | 280-360 |
|  | Thermal Conductivity | W/m=K @ R.T. | ASTM C408 | 35.00 | 82.30 | 20.00 | 1.98 | 1.46 | 3.50 | 41.00 | 27.00 | 2.90 | 2.70 |
|  | Coefficient of Linear Thermal Expansion | m/m-¡C (-25¡C through ²1000¡C) | ASTM C372 | 8.40 | 4.6-5.7 | 1.0-2.0 | 3.60 | 6.3-9.7 | 5.30 | 5.12 | 3.40 | 7.00 | 11.00 |
|  | Specific Heat | cal/g-¡C @ R.T. | ASTM C351 | 0.21 | 0.25 | 0.19 | 0.20 | 0.19 | 0.23 | 0.15 | 0.17 | 0.22 | 0.10 |
|  | Dielectric Constant | 1Mhz @ R.T. | ASTM D150 | 9.60 | 8.0-9.1 | 4.08 | 5.30 | 6.03 | 6.00 | 10.20 | 7.00 | 6.30 | 26@1000kHz |
|  | Dielectric Strength | kV/mm | ASTM D116 | 15.0 | 15.0 | 374.0 | 0.1 | 40.0 | 9.8 | - | 17.7 | 9.3 | 9.0 |
|  | Electrical Resistivity | Wcm @ R.T. | ASTM D1829 | 1014 | 1014 | 1013 | 1014 | >1017 | 1013 | 108 | 1013 | 104 | >1013 |

|  |  | The information supplied is not a warranty or representation by Professional Plastics, Inc. User assumes legal responsibility to test the product for suitability in their particular application. Data is offered solely for your consideration, investigation and verification. All risk of use, singly or in combination with other products, whether or not in accordance with the instructions, directions or suggestions is borne by the user. |
| --- | --- | --- |

Call Professional Plastics at (800) 966-7767 or

E-Mail sales@proplas.com

Order Online at www.professionalplastics.com