Chemical Resistance Chart

Medium Concentration PVC PE PP ABS Acetic acid, Aqueous 25% 60 60 82 N CH3COOH 40% - - - - 60% 23 23 82 N 85% 23 23 49 N Ammonium Sulfate (Alum) AINH4(SO4)2 I2H2O Sat'd 60 60 60 - Ammonium Hydroxide 10% 60 60 100 49 NH4OH 30% - R to 60 - - Ammonium Nitrate NH4NO3 Sat'd 60 60 100 49 Ammonium Phosphate (Monobasic) NH4H2PO4 All 60 60 100 49 Ammonium Sulfate (NH4)2SO4 Sat'd 60 60 100 49 Borax Na3B4O7O10H2O Sat'd 60 60 100 71 Calcium Carbonate CaCO3 Sat'd 60 60 82 - Calcium Chloride 5% - - - - CaCl2 Sat'd 60 60 82 49 Calcium Hypochlorite 30% 60 60 60 71 Ca(OCl)2 Sat'd - - - - CuSO4 o5H2O Sat'd 60 60 49 49 Chlorine Gas (Moisture Content) 0-20 ppm C to 23 C to 23 N N 20 - 50 ppm N C to 23 N N 50+ ppm N C to 23 N N Chlorine Liquid N N N N Chlorinated Water 10 ppm 60 60 82 - Chlorinated Water Sat'd 60 C to 49 82 - Detergents - 60 R to 60 82 - Ferrous Sulphate FeSO4 - 60 60 60 71 Hydrochloric Acid 1% - - - - HCl 10% 60 60 60 C to 49 20% - - - - 30% 60 60 60 C to 23 Conc. - - - - Hypochlorous Acid 10% 60 60 23 23 HOCl 70% - - - - Nitric Acid 5% - - - - HNO3 10% 60 23 82 C to 23 20% - - - - 30% 60 23 60 N 35% - - - - 40% 60 23 23 N 50% 38 C to 23 N N 70% 23 C to 23 N N 100% N N N N Lubricating Oil - 60 23 C to 60 - Phosphoric Acid 10% 60 60 100 - H3PO4 50% 60 60 100 - 85% 60 23 100 23 98% - - - - Potassium Permanganate 10% 23 60 82 - KmnO4 25% 23 60 23 - Soap - 60 R to 60 60 23 Sodium Bicarbonate NaHCO3 - 60 60 100 23 Sodium Carbonate Na2CO3 - 60 60 100 23 Sodium Chloride NaCl - 60 60 100 49 Sodium HypoChlorite NaOClO 5H2O - 60 60 100 49 Sulfur S - 60 60 100 - Sulphuric Acid 30% 60 60 82 49 H2SO4 50% 60 49 82 23 60% 60 49 23 C to 23 70% 60 R to 49 23 C to 23 80% 60 R to 49 82 C to 23 90 23 49 66 C to 23% 93% 23 C to 23 C to 23 N 94% - 98% N C to 23 C to 23 N 100% N C to 23 C to 23 N Urea - 60 60 82 - Urine - 60 60 82 71 Water, Acid Mild H2O - 60 60 60 71 Water, Deionized H2O - 60 60 60 71 Water, Distilled H2O - 60 60 100 71 Water, Potable H2O - 60 60 100 71 Water, Salt H2O - 60 60 100 71 Water, Sea H2O - 60 60 100 71 Water, Soft H2O - 60 60 100 71 Zinc Sulphate - 60 60 82 71

Resistance Code

Code Meaning Typical Result 60 Plastic type is generally resistant to temperature (ºC) indicated by code. Swelling < 3% or weight loss < 0.5% and elongation at break not significantly changed. R to 23 Plastic type is generally resistant to temperature (ºC) indicated by code and may have limited resistance at higher temperatures. Swelling < 3% or weight loss < 0.5% and elongation at break not significantly have limited resistance at higher temperatures. changed. C to 23 Plastic type is generally resistant to temperature (ºC) indicated by code and may be suitable for some conditions Swelling 3-8% or weight loss < 0.5-5% and / or elongation at break decreased by suitable for some conditions. < 50%. N Plastic type is not resistant. Swelling < 8% or weight loss < 5% and / or elongation at break decreased by > 50%. -- Data not available Chemicals that to do not normally affect the properties of an unstressed thermoplastic may cause completely different behavior (such as stress cracking) when under thermal or mechanical stress (such as constant internal pressure or frequent thermal or mechanical stress cycles). Unstressed immersion test chemical resistance information is applicable only when the thermoplastic pipe will not be subject to mechanical or thermal stress that is constant or cycles frequently. When the pipe will be subject to a continuous applied mechanical or thermal stress or to combinations of chemicals, testing that duplicates the expected field conditions as closely as possible should be performed on representative samples of the pipe product to properly evaluate plastic pipe for use in this application.

Call Professional Plastics at (800) 966-7767 or

E-Mail sales@proplas.com

Order Online at www.professionalplastics.com