(FILLED PTFE) COMPOSITIONS & FILL DESCRIPTIONS

| CONSISTS OF | DEFINITION OF FILL |
| --- | --- |
| 5% Glass Fiber 10% Glass Fiber 15% Glass Fiber 20% Glass Fiber 25% Glass Fiber 30% Glass Fiber | Milled glass fibers have the least effect on chemical and electrical properties and add greatly to the mechanical properties of unfilled PTFE. Addition of glass improves compressive properties by as much as 40% and improves wear resistance greatly. These compounds resist acids and oxidation but can be attacked by alkali. |
| 30% Graphite 5% Graphite 10% Graphite 15% Graphite 20% Graphite 25% Graphite | Graphite has good chemical resistance to corrosive environments and exhibits good initial wear and rubbing/sliding characteristics in dry and water applications. Commonly blended with carbon and PTFE. |
| 25% Bronze 40% Bronze 60% Bronze | This filler has better wear, creep resistance, and higher thermal conductivity than glass fiber with PTFE. The compound is easily machined, but has poor chemical resistance in the presence of acids and alkali. Useful in applications which undergo high mechanical loads or high-speed rubbing contacts where the bronze filler supplies the strength and conductivity to carry away excess, unwanted heat. |
| 5% Molybdenum Disulfide | This filler is used frequently in combination with others to increase surface hardness, stiffness, and to reduce the starting coefficient of friction and steady-state wear. Its effect on electrical and chemical properties is negligible. |
| 5% Carbon 10% Carbon 15% Carbon 20% Carbon 25% Carbon 33% Carbon | Carbon has good chemical resistance to corrosive environments. It exhibits good initial wear and rubbing or sliding contact characteristics, both dry and water applications. It is frequently used in piston rings to reduce cylinder wall wear by entrapping abrasive foreign particles in their relatively soft surfaces. |
| 10% Carbon-Graphite 20% Carbon-Graphite 25% Carbon Graphite | These fillers are used both separately and together in PTFE compounds. |
| 5% Calcium Fluoride 10% Calcium Fluoride 15% Calcium Fluoride | ALTERNATIVE TO GLASS FILL. |
| 15% Glass Fiber, 5% Moly 20% Glass Fiber, 5% Moly, 5% Carbon-Graphite 23% Glass Fiber, 2% Moly 25% Glass Fiber, 5% Moly | SEE ABOVE FOR INDIVIDUAL DEFINITIONS. |
| 10% Glass Fiber, 10% Graphite 5% Glass Fiber, 5% Graphite 20% Glass Fiber, 5% Graphite | SEE ABOVE FOR INDIVIDUAL DEFINITIONS. |
| 10% Glass Fiber, 5% Carbon 5% Glass Fiber, 10% Carbon | SEE ABOVE FOR INDIVIDUAL DEFINITIONS. |
| 40% Bronze, 5% Moly 40% Bronze, 10% Moly 55% Bronze, 5% Moly 65% Bronze, 5% Moly | SEE ABOVE FOR INDIVIDUAL DEFINITIONS. |

| TYPICAL PHYSICAL PROPERTIES OF VIRGIN PTFE PRODUCTS |
| --- |
| PTFE Material | Virgin | Virgin "Super" PTFE | Reprocessed | Virgin PTFE blended with: |
| Filler | None | None | None | Glass Fiber | Bronze | Graphite | Carbon | Glass, MoS2 |
| Filler Content By Weight | 0% | 0% | 0% | 25% | 40% | 10% | 10% | 23%, 2% |
| PROPERTIES |
| Specific Gravity | 2.16 | 2.16 | 2.16 | 2.22 | 3.30 | 2.13 | 2.13 | 2.25 |
| Tensile Strength @ Break (PSI) | 3,000 | 4,500 | 1,500 | 2,500 | 2,300 | 2,700 | 2,800 | 2,500 |
| Elongation @ Break | 200% | 800% | 75% | 50% | 60% | 60% | 50% | 50% |
| Shore D Hardness | 54 | 54 | 56 | 63 | 65 | 57 | 62 | 64 |
| Dielectric (Volts/Mil) | 1300 | 2100 | 600 | - | - | - | - | - |

COMMON SPECIFICATIONS FOR Teflon ® AND PTFE PRODUCTS

| Specifications *AMS 3651 AMS 3652 AMS 3656 AMS 3658 AMS 3659 AMS 3660 AMS 3661 AMS 3662 AMS 3667 AMS 3668 AMS 3669 AMS 2491 *MIL-P-22241 *MIL-P-19468 ASTM D1710 ASTM D3293 ASTM D3294 ASTM D3308 | Type Of Specification for PTFE and Teflon ® PTFE RODS, TUBES, SHEETS, SHAPES (See AMS 3652 thru AMS 3669) PTFE FILM PTFE EXTRUSIONS PTFE EXTRUSIONS PTFE EXTRUSIONS PTFE MOLDINGS PTFE FILM PTFE FILM PTFE SHEET, MOLDED PTFE MOLDINGS PTFE SHEET, MOLDED SURFACE TREATMENT OF PTFE PTFE SHEET & FILM (See ASTM D3293 & ASTM D3308) PTFE RODS, MOLDED & EXTRUDED (See ASTM-D1710) PTFE ROD PTFE MOLDED SHEET PTFE MOLDED SHEET OR SHAPES PTFE SKIVED TAPE |
| --- | --- |
| * Note: These specifications have been deleted. See replacement specifications for current information. |

Call Professional Plastics at (800) 966-7767 or

E-Mail sales@proplas.com

Order Online at www.professionalplastics.com