#### Kynar® 740/1000HD PVDF Homopolymer, Compression Molded

Subcategory: Fluoropolymer; Polymer; PVDF; Thermoplastic

Material Notes: 
Compression molded, manufactured from Kynar polyvinylidene fluoride resin. This material offers excellent corrosion and chemical resistance at both ambient and elevated temperatures. PVDF is also inherently UV stable, mechanically tough, abrasion and flame resistant. Kynar 1000HD is a whiter grade of PVDF than Kynar 740.

Kynar® is a trade name of Elf Atochem North America.

| Physical Properties | Metric | English | Comments |
| --- | --- | --- | --- |
| Density | 1.78 g/cc | 0.0643 lb/in³ | ASTM D792 |
| Water Absorption | 0.03 % | 0.03 % | ASTM D570; 24 hrs. |
| Mechanical Properties |
| Hardness, Shore D | 77 | 77 | ASTM D2240 |
| Tensile Strength @ Yield | 48.3 MPa | 7000 psi | ASTM D638 |
| Elongation at Break | 100 % | 100 % | ASTM D638 |
| Elongation at Yield | 7 - 13 % | 7 - 13 % | ASTM D638 |
| Tensile Modulus | 1.72 GPa | 250 ksi | ASTM D638 |
| Flexural Modulus | 2 GPa | 290 ksi | ASTM D790 |
| Flexural Yield Strength | 55.2 MPa | 8000 psi | ASTM D790 |
| Izod Impact, Unnotched | 10.7 - 42.7 J/cm | 20 - 80 ft-lb/in | ASTM D256 |
| Izod Impact, Notched | 1.6 J/cm | 3 ft-lb/in | ASTM D256 |
| Electrical Properties |
| Volume Resistivity | 2e+014 ohm-cm | 2e+014 ohm-cm | ASTM D257 |
| Dielectric Constant | 8.5 | 8.5 | ASTM D150; at 1kHz |
| Dielectric Strength | 160 kV/mm | 4060 kV/in | ASTM D149 |
| Thermal Properties |
| CTE, linear 68°F | 119 µm/m-°C | 66 µin/in-°F | ASTM D696 |
| Deflection Temperature at 0.46 MPa (66 psi) | 125 - 140 °C | 257 - 284 °F | ASTM D648 |
| Deflection Temperature at 1.8 MPa (264 psi) | 110 °C | 230 °F | ASTM D648 |
| Flammability, UL94 | V-0 | V-0 |  |