# Kynar ® 2:1 Shrink Tubing

Description: Kynar 2:1 Shrink Tubing is made from an irradiated modified Polyvinylidene Fluoride (Kynar®).  This thin walled heat shrink tubing offers mechanical strength and high-temperature properties. It has high abrasion resistance and dielectric strength combined with resistance to most industrial chemicals.  When heated above 175°C, shrinks to form a skintight cover. 
It is rated for -55°C to 175°C continuous operation.  The tubing is transparent and is ideal for use as a component jacket.

Specifications: MIL-I-23053/8; AMS-3632; UL.

Material: Kynar®, Shrink Ratio 2:1.

Temperature Rating: -55°C To 175°C.

Standard Color: Clear.
Other colors available subject to minimum quantities.

Packaging: 4 Foot Lengths.*  *ALSO  AVAILABLE AS CUT PIECES,  UPON REQUEST.

| Order Size | Expanded I.D. (Minimum) | Recovered I.D. (Maximum) | Recovered Wall (Nominal) | Kynar Shrink Tubing |
| --- | --- | --- | --- | --- |
| in. | in. | (mm) | in. | (mm) | in. | (mm) |  |
| 3/64 | .046 | (1,17) | .023 | (0,58) | .010 | (0,25) | Kynar Heat Shrink Tubing |
| 1/16 | .063 | (1,60) | .031 | (0,79) | .010 | (0,25) |  |
| 3/32 | .093 | (2,36) | .046 | (1,17) | .010 | (0,25) | Kynar Heat Shrink Tubing |
| 1/8 | .125 | (3,18) | .062 | (1,57) | .010 | (0,25) |  |
| 3/16 | .187 | (4,75) | .093 | (2,36) | .010 | (0,25) | Kynar Heat Shrink Tubing |
| 1/4 | .250 | (6,35) | .125 | (3,18) | .012 | (0,30) |  |
| 3/8 | .375 | (9,53) | .187 | (4,75) | .012 | (0,30) | Kynar Heat Shrink Tubing |
| 1/2 | .500 | (12,70) | .250 | (6,35) | .012 | (0,30) |  |
| 5/8 | .625 | (15,88) | .313 | (7,94) | .014 | (0,36) | Kynar Heat Shrink Tubing |
| 3/4 | .750 | (19,05) | .375 | (9,53) | .017 | (0,43) |  |
| 1 | 1.000 | (25,40) | .500 | (12,70) | .019 | (0,48) | Kynar Heat Shrink Tubing |
| 1-1/2 | 1.500 | (38,10) | .750 | (19,05) | .020 | (0,51) |  |
| 2 | 2.000 | (50,80) | 1.000 | (25,40) | .022 | (0,56) |  |

| Physical Properties Tensile Strength: 5500 PSI Ultimate Elongation: 350% Longitudinal Change: +1,-10% Specific Gravity: 1.7 Low Temperature Flexibility (4 HRS @ -55°C): No Cracking Flammability: Self Extinguish Meets UL 224 VW-1 Test | Electrical Properties Dielectric Strength: 900 V/Mil Volume Resistivity: 1014 Ohm-cm Chemical Properties Corrosive Effect: Non-Corrosive Fuel & Oil Resistance: Excellent Solvent Resistance: Excellent Abrasion Resistance: Excellent Acid Resistance: Excellent Alkali Resistance: Excellent Fungus Resistance: Non-Nutrient |
| --- | --- |

PROPERTIES INFORMATION IS TYPICAL DATA ONLY
AND SHOULD NOT BE USED FOR SPECIFICATION REQUIREMENTS.

Call Professional Plastics at (800) 966-7767 or

E-Mail sales@proplas.com

Order Online at www.professionalplastics.com