MYLAR® A 

Product Description

Mylar® A films are tough, general purpose films that are transparent in 48 through 92 gauge and translucent in heavier gauges. They have a rough surface to provide ease of handling, good adhesion, and processability. They are used for a broad range of industrial applications.

General Product Info

Mylar® A films have balanced tensile properties and excellent resistance to moisture and most chemicals. They can withstand temperature extremes from -100°F to 300ºF. Mylar® does not become brittle with age under normal conditions, because it contains no plasticizers.

Special Features

Slit rolls are available in the following ID and OD configuration: 3" ID 9 1/2" OD 3" ID 13" OD 3" ID 16" OD 3" ID 18" OD 6" ID 11" OD 6" ID 14" OD 6" ID 16 1/2" OD 6" ID 18" OD Master rolls are much longer lengths, splice free, and are available on 6 inch and 10 inch ID cores. Master rolls are available in minimum order quantities of 10,000 pounds per item.

Typical Applications

Mylar® A films are used extensively in a wide variety of markets. Some of them are: Apparel stays Book jackets Carbon ribbon Control Tape Drumheads Duct Liners Identifications Membrane touch switches Metallized Base Pressure Sensitive Labels (plain or metallized) Protective surfacing Release liners Roll leaf (hot stamping) Spirit Masters

Approvals

FDA Food Contact Status - All gauges of Mylar® A comply with the Food and Drug Administration regulation 21 CFR 177.1630 -- Polyethylene phthalate polymers. This regulation describes films which may be safely used in contact with all types of food excluding alcoholic beverages. Uncoated films such as Mylar® A can be used to contain foods during oven cooking or oven baking at temperatures above 250 °F. UL 94 VTM-2 - for 92-1400 gauge (0.023 - 0.35mm) UL Recognition - for 92-500 gauge (0.023-0.13mm) HWI=5, HAI=4, CTI=1; for 700-1400 gauge (0.18-0.35mm) HWI=4, HAI=0, CTI=1

Typical Properties

Available Thickness [Gauge] 48; 75; 92; 142; 200; 300; 400; 500; 750; 900; 1000; 1200; 1400

Property Thickness Value Units Test OPTICAL Haze 48 4 % ASTM D1003 Haze 75 15 % ASTM D1003 Haze 92 16 % ASTM D1003 Haze 142 9 - 29 % ASTM D1003 Haze 200 13 - 37 % ASTM D1003 Haze 300 14 - 50 % ASTM D1003 Haze 400 20 - 55 % ASTM D1003 Haze 500 21 - 60 % ASTM D1003 PHYSICAL Elongation at Break MD 48 110 % ASTM D882A Elongation at Break MD 75 110 % ASTM D882A Elongation at Break MD 92 110 % ASTM D882A Elongation at Break MD 142 125 % ASTM D882A Elongation at Break MD 200 135 % ASTM D882A Elongation at Break MD 300 135 % ASTM D882A Elongation at Break MD 400 140 % ASTM D882A Elongation at Break MD 500 140 % ASTM D882A Elongation at Break MD 750 140 % ASTM D882A Elongation at Break MD 900 150 % ASTM D882A Elongation at Break MD 1000 150 % ASTM D882A Elongation at Break MD 1400 170 % ASTM D882A Elongation at Break TD 48 70 % ASTM D882A Elongation at Break TD 75 90 % ASTM D882A Elongation at Break TD 92 90 % ASTM D882A Elongation at Break TD 142 100 % ASTM D882A Elongation at Break TD 200 110 % ASTM D882A Elongation at Break TD 300 110 % ASTM D882A Elongation at Break TD 400 115 % ASTM D882A Elongation at Break TD 500 115 % ASTM D882A Elongation at Break TD 750 115 % ASTM D882A Elongation at Break TD 900 130 % ASTM D882A Elongation at Break TD 1000 140 % ASTM D882A Elongation at Break TD 1400 170 % ASTM D882A Modulus 48 - 1400 507 kpsi ASTM D822 Tensile Strength MD 48 26 kpsi ASTM D882A Tensile Strength MD 75 28 kpsi ASTM D882A Tensile Strength MD 92 28 kpsi ASTM D882A Tensile Strength MD 142 28 kpsi ASTM D882A Tensile Strength MD 200 28 kpsi ASTM D882A Tensile Strength MD 300 27 kpsi ASTM D882A Tensile Strength MD 400 26 kpsi ASTM D882A Tensile Strength MD 500 27 kpsi ASTM D882A Tensile Strength MD 750 27 kpsi ASTM D882A Tensile Strength MD 900 27 kpsi ASTM D882A Tensile Strength MD 1000 27 kpsi ASTM D882A Tensile Strength MD 1400 26 kpsi ASTM D882A Tensile Strength TD 48 32 kpsi ASTM D882A Tensile Strength TD 75 34 kpsi ASTM D882A Tensile Strength TD 92 34 kpsi ASTM D882A Tensile Strength TD 142 34 kpsi ASTM D882A Tensile Strength TD 200 33 kpsi ASTM D882A Tensile Strength TD 300 31 kpsi ASTM D882A Tensile Strength TD 400 30 kpsi ASTM D882A Tensile Strength TD 500 30 kpsi ASTM D882A Tensile Strength TD 750 30 kpsi ASTM D882A Tensile Strength TD 900 29 kpsi ASTM D882A Tensile Strength TD 1000 29 kpsi ASTM D882A Tensile Strength TD 1400 25 kpsi ASTM D882A Yield (nominal) 48 41,300 in²/lb Yield (nominal) 75 26,500 in²/lb Yield (nominal) 92 21,500 in²/lb Yield (nominal) 142 14,000 in²/lb Yield (nominal) 200 9,900 in²/lb Yield (nominal) 300 6,600 in²/lb Yield (nominal) 400 5,000 in²/lb Yield (nominal) 500 4,000 in²/lb Yield (nominal) 750 2,600 in²/lb Yield (nominal) 900 2,200 in²/lb Yield (nominal) 1000 2,000 in²/lb Yield (nominal) 1400 1,400 in²/lb THERMAL Shrinkage MD (150°C) 48 2.0 % Unrestrained @ 150°C/30 min Shrinkage MD (150°C) 75 2.0 % Unrestrained @ 150°C/30 min Shrinkage MD (150°C) 92 1.9 % Unrestrained @ 150°C/30 min Shrinkage MD (150°C) 142 1.5 % Unrestrained @ 150°C/30 min Shrinkage MD (150°C) 200 1.3 % Unrestrained @ 150°C/30 min Shrinkage MD (150°C) 300 1.2 % Unrestrained @ 150°C/30 min Shrinkage MD (150°C) 400 1.1 % Unrestrained @ 150°C/30 min Shrinkage MD (150°C) 500 1.1 % Unrestrained @ 150°C/30 min Shrinkage MD (150°C) 750 1.6 % Unrestrained @ 150°C/30 min Shrinkage MD (150°C) 900 1.6 % Unrestrained @ 150°C/30 min Shrinkage MD (150°C) 1000 1.5 % Unrestrained @ 150°C/30 min Shrinkage MD (150°C) 1400 1.3 % Unrestrained @ 150°C/30 min Shrinkage TD (150°C) 48 1.0 % Unrestrained @ 150°C/30 min Shrinkage TD (150°C) 75 1.1 % Unrestrained @ 150°C/30 min Shrinkage TD (150°C) 92 1.1 % Unrestrained @ 150°C/30 min Shrinkage TD (150°C) 142 1.0 % Unrestrained @ 150°C/30 min Shrinkage TD (150°C) 200 0.8 % Unrestrained @ 150°C/30 min Shrinkage TD (150°C) 300 0.8 % Unrestrained @ 150°C/30 min Shrinkage TD (150°C) 400 0.7 % Unrestrained @ 150°C/30 min Shrinkage TD (150°C) 500 0.7 % Unrestrained @ 150°C/30 min Shrinkage TD (150°C) 750 0.9 % Unrestrained @ 150°C/30 min Shrinkage TD (150°C) 900 1.1 % Unrestrained @ 150°C/30 min Shrinkage TD (150°C) 1000 1.1 % Unrestrained @ 150°C/30 min Shrinkage TD (150°C) 1400 0.8 % Unrestrained @ 150°C/30 min

Standard Put-ups

Core I.D. (Inches) Roll O.D. (Inches) Thickness (Gauge) Length (Feet) 3 9 1/2 48 10,500 3 9 1/2 75 6,700 3 9 1/2 92 5,400 3 9 1/2 142 3,500 3 9 1/2 200 2,500 3 9 1/2 300 1,650 3 9 1/2 400 1,250 3 9 1/2 500 1,000 3 9 1/2 750 650 3 9 1/2 900 550 3 9 1/2 1000 500 3 9 1/2 1400 350

Contact Info

Professional Plastics, Inc.

1810 East Valencia Drive

Fullerton, CA 92831- USA

(800) 966-7767  Fax (866) 776-7527

sales@proplas.com

www.professionalplastics.com

Disclaimer

Note: These values are typical performance data for DuPont Teijin Films' polyester film; they are not intended to be used as design data. We believe this information is the best currently available on the subject. It is offered as a possible helpful suggestion in experimentation you may care to undertake along these lines. It is subject to revision as additional knowledge and experience is gained. DuPont Teijin Films makes no guarantee of results and assumes no obligation or liability whatsoever in connection with this information. This publication is not a license to operate under, or intended to suggest infringement of, any existing patents. CAUTION: Do not use in medical applications involving permanent implantation in the human body DuPont Teijin Films accepts no liability for use of it's products in medical applications not reviewed and approved by DuPont Teijin Films or for product misuse. DuPont Teijin Films supplies products to an agreed specification and does not manufacture products designed specifically for medical end use. Melinex®, Mylar®, and Cronar® are registered trademarks of DuPont Teijin Films U.S. Limited Partnership. Teijin® and Tetoron® are registered trademarks of Teijin Limited and are licensed to DuPont Teijin Films U.S. Limited Partnership. Teonex® is a registered trademark of Teijin DuPont Films Japan Limited and is licensed to DuPont Teijin Films U.S. Limited Partnership.

# Call Professional Plastics at (800) 966-7767 or

# E-Mail sales@proplas.com

# Order Online at www.professionalplastics.com