Mylar D Polyethylene Terephthalate (PET) Description Mylar D is a clear, brilliant film which is surface treated on both sides to give superior slip characteristics and excellent handling properties Applications , Archival, Graphics, Safety Film, Decorating for laminates, Report covers, microfilm, layout base, membrane switches, protective glazing, labels, overhead transparancies, stationery supplies, graphic arts Pre-treatment Slip Treated Approvals Approved by the US Library of Congress for Archival and Conservation applications Properties Unit Test Method Other - um Micrometer method 75 100 125 - gauge 300 400 500 - " .003 .004 .005 Substance Yield g/M2 g/M2 105 141 175 Yield M2/ Kg M2/Kg 9.5 7.1 5.7 Optical Properties Haze 75 mic % ASTM D 1003 0.3 - - - Haze 100 mic % ASTM D 1003 0.4 - - - Haze 125 mic % ASTM D 1003 0.5 - - - Total Transmission 75 mic % ASTM D 1003 90 - - - Total Transmission 100 mic % ASTM D 1003 90 - - - Total Transmission 125 mic % ASTM D 1003 90 - - - Coefficient of Friction* 75 mic Static ASTM D 0.40 ASTM D1894D1 0.50 - - Coefficient of Friction* 100 mic Static ASTM D 0.40 ASTM D1894D1 0.50 - - Coefficient of Friction* 125 mic Static ASTM D 0.40 ASTM D1894D1 0.50 - - Dimensional Stability 75 mic - - 150°C (302°F)/30 min MD 1.5 TD 0.5 - Dimensional Stability 100 mic - - 150°C (302°F)/30 min MD 1.5 TD 0.5 - Dimensional Stability 125 mic - - 150°C (302°F)/30 min MD 1.5 TD 0.5 - Tensile Strength kgf/mm2 20 ASTM D 882A (kpsi) 28 - - - Tensile Strength kgf/mm2 20 ASTM D 882A (kpsi) 28 - - - Tensile Strength kgf/mm2 20 ASTM D 882A (kpsi) 28 - - - * Film to Film Other : Available also in 175 and 250 mic {Mylar D is no longer manufactured although we still hold limited stocks} Thr brilliance and clarity of Mylar D film enhance the appearance of some end products, and its toughness and dimensional stability help ensure a long and troublefree service life. Specifically designed for metallising applications where metallised brilliance is required. Other uses include labels, decals, over-laminates and decorative laminations where superior optical characterisitics are essential. Disclaimer All technical information and related data supplied is believed to be accurate and complete. However, it will remain the responsibility of the purchaser / user to determine the suitability of each product for a particular application and shall assume all risk and liability in connection therewith. No warranty is implied with regard to information or recommendations given by our distributors and or subcontractors. The descriptions of products and services displayed on this web site and the terms under which they are given may be modified at any time without notice. In any event or occurrence, our liability is strictly limited to the value of the original invoice. Any links on this site are for the convenience of the visitor only and we are not responsible for their content. Mylar® brand polyester film. Melinex® and Mylar® are registered trademarks of DuPont Teijin Films.

# Call Professional Plastics at (800) 966-7767 or

# E-Mail sales@proplas.com

# Order Online at www.professionalplastics.com