| Specific Gravity | 1.15 g/cm3 |
| --- | --- |
| Tensile Strength | 10,500 - 12,000 (psi) |
| Compressive Strength @ 10% Deflection | 15,000 (psi) |
| Elongation | 30 - 40 % |
| Tensile Modulus | 460,000 (psi) |
| Tensile Impact, 73°F | 80 - 130 ft. lbs./ in. |
| Flexural Strength | 17,000 (psi) |
| Flexural Modulus | 330,000 (psi) |
| Coefficient of Friction | .36 - .42 (dry vs. Steel) |
| 24 Hour H2O | .5 % |
| Equilibrium H2O | 1.25 - 4 % |
| Hardness | 80 (Scale D) |
| Coefficient of Thermal Expansion | 5.5 x 10 (-5) in./in./F |
| Continuous Operating Temp | 220 - 250 Degrees F |

Nylon®  MD Material Data Sheet

# Text boxes

Need help with your order? Call us at 1-800-966-PROS 
or order online at www.professionalplastics.com today!