| Properties | NEMA grade reinforcement~ resin binder | G-10/FR4 glass~ epoxies | X paper~ phenolic | C, CE canvas~ phenolic | L, LE linen~ phenolic |
| --- | --- | --- | --- | --- | --- |
| Tensile Strength |
| lengthwise, PSI | 40,000 | 20,000 | 9,500 | 12,500 |
| crosswise, PSI | 35,000 | 16,000 | 7,500 | 8,750 |
| Compressive Strength |
| flatwise, PSI | 60,000 | 36,000 | 37,000 | 37,000 |
| edgewise, PSI | 35,000 | 19,000 | 23,500 | 25,000 |
| Flexural Strength |
| lengthwise, PSI | 55,000 | 25,000 | 17,000 | 15,000 |
| crosswise, PSI | 45,000 | 22,000 | 15,000 | 13,750 |
| Properties | NEMA grade reinforcement~ resin binder | FR4 glass~ epoxies | X paper~ phenolic | C, CE canvas phenolic | L, LE linen~ phenolic |
| Modulus of Elasticity in flex |
| lengthwise, PSI x 10 6 | 2.7 | 1.8 | .95 | 1.05 |
| crosswise, PSI x 10 6 | 2.2 | 1.3 | .85 | .85 |
| Shear Strength, PSI | 19,000 | 12,000 | 11,500 | 11,750 |
| IZOD Impact |
| flatwise, ft lb per inch of notch | 7 | 4 | 3.2,2.3 | 2.5,1.8 |
| edgewise, ft lb per inch of notch | 5.5 | 0.5 | 1.9,1.4 | 1.1, 1 |
| Rockwell Hardness M scale | 110 | 110 | 104 | 105 |
| Specific Gravity | 1.82 | 1.36 | 1.35 | 1.34 |
| Coefficient of Thermal Expansion |
| cm/cm/ deg C x 10 -5 | .9 | 6 | 2 | 2 |
| Properties | NEMA grade reinforcement~ resin binder | FR4 glass~ epoxies | X paper~ phenolic | C, CE canvas phenolic | L, LE linen~ phenolic |
| Water Absorption |
| .062" thick, % per 24 hrs | 0.25 | 6 | 4.4,2.2 | 2.5,1.95 |
| .125" thick, % per 24 hrs | 0.15 | 3.3 | 2.5,1.6 | 1.6,1.3 |
| .500" thick, % per 24 hrs | 0.10 | 1.1 | 1.2,0.75 | 0.9,0.7 |
| Dielectric Strength, volt/mil |
| perpendicular to laminations; short |
| .062" thick | 500 | 700 | 200\500 | 200\500 |
| .125" thick | 400 | 500 | 150\360 | 150\360 |
| Dissipation Factor |
| condition A, 1 megacycle | 0.025 | 0.06 | 0.1,.055 | 0.1,.055 |
| Dielectric Constant |
| condition A, 1 megacycle | 5.2 | 6 | - , 5.8 | - , 5.8 |
| Properties | NEMA grade reinforcement~ resin binder | FR4 glass~ epoxies | X paper~ phenolic | C, CE canvas phenolic | L, LE linen~ phenolic |
| Insulation Resistance |
| Condition: 96 hours at 90% relative humidity (in mega ohms) | 200,000 | - | - | - |
| Flame Resistance |
| Underwriter Labs, Classification | 94V-0 | 94HB | 94HB | 94HB |
| Bond Strength, in lbs | 2,000 | 700 | 1,800 | 1,600 |
| Max Continuous Operating Temperature |
| Approximate degrees F | 285 | 285 | 265 | 265 |
| Sheet Mil Spec: Mil-I-24768 / _ _ | 27 | 12 | 14 | 13 |
| Types | GEE-F | PBM | FBG | FBE |
| The above information is provided for informational purposes only. We believes this data to be reliable but disclaims any liability for damages or injury which results from the use of this data and nothing contained herein shall constitute a guarantee, warranty (including warranty of merchantability) or representation (including freedom from patent liability) by Professional Plastics with respect to the data, the products described, or their use for any particular purpose, even if that purpose is known to Professional Plastics. |

# Text boxes

Need help with your order? Call us at 1-800-966-PROS 
or order online at www.professionalplastics.com today!