SIMONA® Fire Safe Products

SIMONA® PVC-C CORZAN® FM 4910 G2

| Fabricators & Specifiers Benefits FM 4910 listed chemical-grade CPVC Outstanding impact resistance Excellent high-temperature distortion resistance Temperature range from –40°F/–40°C up to +185°F/+85°C Excellent chemical and corrosion resistance Self-extinguishing, flame retardant and smoke reducing Easily fabricated, welded and machined One-side protective foil Accurate to dimensional tolerances |  | Application Areas Semiconductor processing equipment Clean-room technology |
| --- | --- | --- |

| SIMONA® PVC-C CORZAN® FM 4910 G2 Extruded sheets (thickness in inch) |
| --- |
| Size 48" x 96" | 1/32 | 1/16 | 3/32 | 1/8 | 3/16 | 1/4 | 3/8 | 1/2 | 5/8 | 3/4 | 1 | 1 1/4 | 1 1/2 | 1 3/4 | 2 |  |  |
| White 1 side protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Size 60" x 120" | 1/32 | 1/16 | 3/32 | 1/8 | 3/16 | 1/4 | 3/8 | 1/2 | 5/8 | 3/4 | 1 | 1 1/4 | 1 1/2 | 1 3/4 | 2 |  |  |
| White 1 side protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

Call for custom lengths, other sizes, colors or special requirements.

| SIMONA® PVC-C CORZAN® FM 4910 G2 Welding Rods - Available on request |
| --- |
|  | Round |  |  |  |  |  |
| White |  |  |  |  |  |  |

Call for other types, colors or special requirements.

SIMONA® PVC-C CORZAN® FM 4910 G2

Technical Data

Property ASTM* Test Method Unit Typical Value Physical Density D-792 g/cm³ 1.54 Water Absorption(24 hrs @ 73°F) D-570 % NA Mechanical Tensile Strength D-638 PSI 7,500 Tensile Modulus D-638 PSI 320,000 Elongation at break D-638 % 25 Izod Impact D-256 ft. lbs./in. NA Rockwell Hardness D-785 “R” scale NA Thermal Heat Distortion Temperature D-648 at 66 psi D-648 °F NA at 264 psi D-648 °F NA Vicat Softening Temperature D-1525 °F 201 Coefficient of Thermal Expansion D-696 in./in. °C NA Temperature Range °F -40 to +185 Flammability Ratings Flammability FM-4910 listed * American Society of Testing Materials

Standards and Specifications

- FM 4910 listed

Legend:
= Available ex stock
= Available on request


Data and information used the preparation of this sheet have been obtained from controlled laboratory procedures and/or carefully documented empirical observations. As such, they may not be applicable to all uses and conditions. The reader is advised that no guarantees, written or implied, including guarantees as to the fitness for a particular purpose or use, are to be construed from this bulletin. Persons with questions as to the applicability of this material, or SIMONA AMERICA products to specific uses or situations are urged to contact our customer service department.

Call Professional Plastics at (800) 966-7767 or

E-Mail sales@proplas.com

Order Online at www.professionalplastics.com