SIMONA® Homopolymer Polypropylene

SIMONA® VERSADUR® PP-H – 500 Series

SIMONA® PP-DWST

SIMONA® PP-DWU / PP-DWU-SK

SIMONA® PP white

| Fabricators & Specifiers Benefits Excellent chemical and corrosion resistance Easily to fabricate, weld or machine Accurate to dimensional tolerances Stress relieved, square, flat sheets Color consistent Showcase quality surface Meets established ASTM specifications |  | Application Areas Semiconductor processing equipment Machined and fabricated parts Laboratory equipment Wet benches Food grade applications Prosthetics Etching and plating tanks Acid tanks Ducts, fume hoods and other protective equipment |
| --- | --- | --- |

| SIMONA® VERSADUR® PP-H - 500 Series Extruded sheets (thickness in inch) |
| --- |
| Size 48" x 96" | 1/32 | 1/16 | 3/32 | 1/8 | 3/16 | 1/4 | 3/8 | 1/2 | 5/8 | 3/4 | 1 | 1 1/4 | 1 1/2 | 1 3/4 | 2 |  |  |
| 500 Natural smooth finish without protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 500 Natural smooth finish 2 side protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 515 European grey 1 side protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 520 White high gloss without protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 520 White high gloss 2 side protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 530 Black high gloss without protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 530 Black high gloss 2 side protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 540 Blue high gloss 1 side protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Size 48" x 120" |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 500 Natural smooth finish without protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 520 White high gloss 2 side protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

Call for custom lengths, other sizes, colors or special requirements.


Standards and Specifications

- ASTM D-4101 Group I Class I Grade I

- FDA Regulation Title 21 CFR 177.1520 (C1.1)

- Federal Specification LP-394B Type I (GP) Type III Grade IIIA Class III

- USDA Approval for direct contact with meat and poultry products (500 Natural and 520 White)

- Military Standard D/N/A

- California Proposition 65 – Safe Drinking Water and Toxic Enforcement Act – Passes

- UV Radiation Exposure 500 hours no visible change (515 European grey)

- Standards and specifications not valid for 581 Grey Polyester backed

| SIMONA® PP-DWST Extruded sheets (thickness in mm) |
| --- |
| Size 2000 x 1000 mm | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 10 | 12 | 15 | 20 | 25 | 30 | 35 | 40 | 50 |
| 500 Natural smooth finish without protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Size 3000 x 1500 mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 500 Natural smooth finish without protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

Call for custom lengths, other sizes, colors or special requirements.

| SIMONA® PP-DWU Extruded sheets (thickness in mm) |
| --- |
| Size 2000 x 1000 mm | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 10 | 12 | 15 | 20 | 25 | 30 | 35 | 40 | 50 |
| 515 European grey without protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Size 3000 x 1500 mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 515 European grey without protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Size 4000 x 2000 mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 515 European grey without protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

Call for custom lengths, other sizes, colors or special requirements.

| SIMONA® PP white Extruded sheets (thickness in mm) |
| --- |
| Size 2440 x 1220 mm | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 10 | 12 | 15 | 20 | 25 | 30 | 35 | 40 | 50 |
| 520 White 2 side protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

Call for custom lengths, other sizes, colors or special requirements.

| SIMONA® PP-DWU-SK Extruded sheets (thickness in mm) |
| --- |
| Size 2000 x 1000 mm | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 10 | 12 | 15 | 20 | 25 | 30 | 35 | 40 | 50 |
| 581 White polyester-backed without protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Size 3000 x 1500 mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 581 White polyester-backed without protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Size 20,000 x 1500 mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 581 White polyester-backed without protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

Call for custom lengths, other sizes, colors or special requirements.

| SIMONA® PP-DWST Rods (diameter in inch) |
| --- |
| Length: 8 ft | 1/4 | 3/8 | 1/2 | 5/8 | 3/4 | 1 | 1 1/8 | 1 1/4 | 1 3/8 | 1 1/2 | 1 5/8 | 1 3/4 | 1 7/8 | 2 |  |  |  |
| 500 Natural |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Length: 6 ft | 2 1/4 | 2 3/8 | 2 1/2 | 2 3/4 | 3 | 3 1/4 | 3 1/2 | 4 | 4 1/2 | 5 | 5 1/2 |  |  |  |  |  |  |
| 500 Natural |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Length: 4 ft | 6 | 6 1/2 | 7 | 8 | 9 | 10 | 12 | 13 | 14 |  |  |  |  |  |  |  |  |
| 500 Natural |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

Call for custom lengths, other sizes (metric dimensions), colors or special requirements.

| SIMONA® PP-DWST Welding Rods |
| --- |
|  | Round | Triangular (TA 80) | Triangular (TA 90) | Three-core (TL) | Oval | Twin (ZW) |
| 500 Natural |  |  |  |  |  |  |

Call for other types, colors or special requirements.

Legend:
= Available ex stock
= Available on request


Data and information used the preparation of this sheet have been obtained from controlled laboratory procedures and/or carefully documented empirical observations. As such, they may not be applicable to all uses and conditions. The reader is advised that no guarantees, written or implied, including guarantees as to the fitness for a particular purpose or use, are to be construed from this bulletin. Persons with questions as to the applicability of this material, or SIMONA AMERICA products to specific uses or situations are urged to contact our customer service department.

Call Professional Plastics at (800) 966-7767 or

E-Mail sales@proplas.com

Order Online at www.professionalplastics.com