SIMONA® PVC CLEAR

SIMONA® VERSADUR®  Clear PVC Type I

SIMONA® PVC-GLAS

| Fabricators & Specifiers Benefits Normal Impact Excellent chemical and corrosion resistance Easily to fabricate, welded and machined Showcase quality surface Single- or double-side protective masking Stress relieved, square, flat sheet Accurate to dimensional tolerances Color consistent |  | Application Areas Chemical processing Semiconductor processing equipment Machined and fabricated parts Work Stations |
| --- | --- | --- |

| SIMONA® VERSADUR® Clear PVC Type I – 151 Series Extruded sheets (thickness in inch) |
| --- |
| Size 48" x 96" | 1/32 | 1/16 | 3/32 | 1/8 | 3/16 | 1/4 | 3/8 | 1/2 | 5/8 | 3/4 | 1 | 1 1/4 | 1 1/2 | 1 3/4 | 2 |  |  |
| 151 Clear 2 side protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 59" x 118" special quote |

Call for custom lengths, other sizes, colors or special requirements.

Standards and Specifications

- ASTM D-1784-81 Type I Grade I Class 12454

- Federal Specification L-P 535e

- UL 94V-0 Flammability rating

- ASTM E 84 Flame Spread Rate 15, Fuel Contribution 0

- Maximum Application Temperature 140°F

| SIMONA® PVC-GLAS Extruded sheets (thickness in mm) |
| --- |
| Size 2000 x 1000 mm | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 10 | 12 | 15 | 20 | 25 | 30 | 35 | 40 | 50 |
| 151 Clear 2 side protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

Call for custom lengths, other sizes, colors or special requirements.

| SIMONA® PVC-GLAS Welding Rods |
| --- |
|  | Round | Triangular (TA 80) | Triangular (TA 90) |  |  |  |
| 151 Clear |  |  |  |  |  |  |

Call for other types colors or special requirements.

Legend:
= Available ex stock
= Available on request


Data and information used the preparation of this sheet have been obtained from controlled laboratory procedures and/or carefully documented empirical observations. As such, they may not be applicable to all uses and conditions. The reader is advised that no guarantees, written or implied, including guarantees as to the fitness for a particular purpose or use, are to be construed from this bulletin. Persons with questions as to the applicability of this material, or SIMONA AMERICA products to specific uses or situations are urged to contact our customer service department.

Call Professional Plastics at (800) 966-7767 or

E-Mail sales@proplas.com

Order Online at www.professionalplastics.com