SIMONA® Rigid PVC Type II

SIMONA® VERSADUR®  PVC Type II

SIMONA® PVC-MZ

| Fabricators & Specifiers Benefits High Impact (PVC-MZ: Increased Impact) Minimal shrinkage Good corrosion and chemical resistance Easily to fabricate, weld or machine, hot and cold formable Showcase quality surface Stress relieved, square, flat sheets Accurate to dimensional tolerances Color consistent |  | Application Areas Pollution control equipment Machined and fabricated parts Etching and plating tanks Scrubbers, hoods, ducts and other protective equipment |
| --- | --- | --- |

| SIMONA® VERSADUR® PVC Type II – 250 Series Extruded sheets (thickness in inch) |
| --- |
| Size 48" x 96" | 1/32 | 1/16 | 3/32 | 1/8 | 3/16 | 1/4 | 3/8 | 1/2 | 5/8 | 3/4 | 1 | 1 1/4 | 1 1/2 | 1 3/4 | 2 |  |  |
| 250 Light grey without protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 252 White without protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

Call for custom lengths, other sizes, colors or special requirements.

Standards and Specifications

- ASTM D-1784-81 Type II Grade I Class 15333-D

- ASTM E 84 Flame Spread Rate 15, Fuel Contribution 0

- UL 94V Standards

- Federal Specification L-P 535e

| SIMONA® PVC-MZ Extruded sheets (thickness in mm) |
| --- |
| Size 2000 x 1000 mm | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 10 | 12 | 15 | 20 | 25 | 30 | 35 | 40 | 50 |
| 250 Light grey without protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Size 3000 x 1500 mm | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 10 | 12 | 15 | 20 | 25 | 30 | 35 | 40 | 50 |
| 250 Light grey without protective foil |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

Call for custom lengths, other sizes, colors or special requirements.

| SIMONA® PVC-MZ Welding Rods |
| --- |
|  | Round |  |  |  |  |  |
| 250 Light Grey |  |  |  |  |  |  |

Call for custom lengths, other sizes, colors or special requirements.

Legend:
= Available ex stock
= Available on request


Data and information used the preparation of this sheet have been obtained from controlled laboratory procedures and/or carefully documented empirical observations. As such, they may not be applicable to all uses and conditions. The reader is advised that no guarantees, written or implied, including guarantees as to the fitness for a particular purpose or use, are to be construed from this bulletin. Persons with questions as to the applicability of this material, or SIMONA AMERICA products to specific uses or situations are urged to contact our customer service department.

Call Professional Plastics at (800) 966-7767 or

E-Mail sales@proplas.com

Order Online at www.professionalplastics.com