Sumitomo Chemical produces this wholly aromatic polyester family of super heat-resistant engineering plastics.   Sumika Super S1000 series has an operational temperature of 260° C and thermal resistance far exceeding that of  other conventional engineering plastics.  This material will not melt down or  deform its shape even at 400° C.  It is easy to process (milling, drilling) and it is a suitable material for manufacturing parts requiring tight tolerances, such as those needed to produce IC Test Sockets and Nests.

* Sumika Super S1000 is an excellent optional to replace expensive Vespel ® Sockets & Nests.

Thermal Properties                                                                                  Heat Resistance

Continuous use to 260° C

Short term use to 400° C

Low coefficient of linear expansion

Very good dimensional stability

Mechanical Properties

Excellent mechanical properties, even at elevated temperatures.

Creep Resistant

Excellent wear & friction resistance (S1330 grade).

Chemical Properties

High Purity

Moisture resistance ten times greater than polyimide.

Dimensional stability even when exposed to moisture

Resistant to organic solvents and oils.

Flame resistant & even when ignited, major component is CO2.                            Water Absorbtion

Machining

Easily machined to tight tolerances.

Stability allows for tight tolerance microfabrication.

Clean cutting surface, will not melt.

Applications

Parts for BGA,CSP manufacturing and inspection
IC Inspection Connector
Parts for LCD Probe

Glass Handling

Bearings & Thrust Washers

High-Pressure Valve Seat

Piston Rings

Insulator Sleeves

PROFESSIONAL PLASTICS, INC. is the exclusive USA distributor of Sumika Super ® S1000

Comparative Data Sheet

Sumika Super S1000 and Polyimide

Property Test method ASTM Unit Sumika Super S1000 Polyimide Specific Gravity Water Absorption D792 D570 － ％ 1.35 0.04 1.43 0.24 Tensile strength Elongation Flexural strength Flexural modulus Compressive stress(10% strain) Izod impact strength(notched) Rockwell Hardness D638 D638 D790 D790 D695 D256 D785 Mpa ％ Mpa Mpa Mpa J/m － 68.7 8 100 3240 144 22 R124 86.2 7.5 110 3102 133 42 E45-E58 Deflection temperature under load(1.82Mpa) Continuous Use Temp Coefficient of linear thermal expansion D648 - D696 300 260 5.1 360 288 5.4 Volume Resistivity Dielectric Strength Arc Resistance D257 D149 D495 MV/m sec 18 127 (2T)22 230 The above values are for reference and are not guaranteed

Standard Sizes

| Plate Length X Width Thickness 3.93” x 3.93” .196”, .393”, .590” , .787” 2” x 10” .393”, .590” , .787” 9.5” x 4.75” .393” |  | Rod Length 2” 1.57”, 1.97”, 2.36”, 2.75”, 3.15”, 3.93” 39” .393”, .551”, .748”, .945” , 1.18” * other diameters available upon request. |
| --- | --- | --- |

For pricing, questions or material qualification, please contact Professional Plastics, Inc.

PROFESSIONAL PLASTICS, INC.

Leading Supplier of High-Performance Engineering Plastics

(800) 966-7767

www.professionalplastics.com

e-mail: sales@proplas.com

Sumika Super ® S 1000 is a registered tradename of Sumitomo Chemical

Copyright 2006, Professional Plastics, Inc.  All rights reserved