TEONEX® Q72 

Product Description

Teonex® Q72 is biaxially oriented, slightly hazy polyethylene naphthalate (PEN) film. This ulltra thin film which was developed for capacitor applications. It is commercially available in nominal 14 gauge (3.5 micron).

Approvals

UL Component Registration (RTI = 180/160°C) - Relative Thermal Index (RTI) = 180°C (Elect), 160°C (Mech)

Typical Properties

Available Thickness [Gauge] 14

Property Thickness Value Units Test ELECTRICAL Breakdown Voltage 14 330.0 v/µm JIS C-2319 PHYSICAL C.O.F. (dynamic) 14 0.2 ASTM D1894 C.O.F. (static) 14 0.3 ASTM D1894 Density 14 1.36 g/cc Elongation at Break MD 14 74 % ASTM D882-67 (Modified to TDF) Elongation at Break TD 14 73 % ASTM D882-67 (Modified to TDF) Surface Roughness 14 0.074 nm TDF Method (Inside) Surface Roughness 14 1.3 nm TDF Method (Rm) Tensile Strength MD 14 37 kpsi ASTM D882-67 (Modified to TDF) Tensile Strength TD 14 40 kpsi ASTM D882-67 (Modified to TDF) THERMAL Glass Transition (Tg) 14 250 °F DSC Melting Point 14 516 °F DSC Shrinkage MD (150°C) 14 1.0 % JIS C-2318 (Modified to TDF) Shrinkage TD (150°C) 14 1.3 % JIS C-2318 (Modified to TDF)

Contact Info

Professional Plastics, Inc. 1810 E. Valencia Drive Fullerton, CA 92831 – USA Phone (714) 446-6500 Fax (714) 447-0114

Disclaimer

Note: These values are typical performance data for DuPont Teijin Films' polyester film; they are not intended to be used as design data. We believe this information is the best currently available on the subject. It is offered as a possible helpful suggestion in experimentation you may care to undertake along these lines. It is subject to revision as additional knowledge and experience is gained. DuPont Teijin Films makes no guarantee of results and assumes no obligation or liability whatsoever in connection with this information. This publication is not a license to operate under, or intended to suggest infringement of, any existing patents. CAUTION: Do not use in medical applications involving permanent implantation in the human body (DuPont Teijin Films Medical Policy). For other medical applications, see the Medical Caution Statement. DuPont Teijin Films accepts no liability for use of it's products in medical applications not reviewed and approved by DuPont Teijin Films or for product misuse. DuPont Teijin Films supplies products to an agreed specification and does not manufacture products designed specifically for medical end use. Melinex®, Mylar®, and Cronar® are registered trademarks of DuPont Teijin Films U.S. Limited Partnership. Teijin® and Tetoron® are registered trademarks of Teijin Limited and are licensed to DuPont Teijin Films U.S. Limited Partnership. Teonex® is a registered trademark of Teijin DuPont Films Japan Limited and is licensed to DuPont Teijin Films U.S. Limited Partnership.