Ultem® Polyetheride (PEI)

| TYPICAL PROPERTIES of ULTEM® |
| --- |
| ASTM or UL test | Property | Ultem® 1000 unfilled | Ultem® 2300 30% glass |
| PHYSICAL |
| D792 | Density (lb/in³) (g/cm³) | 0.046 1.28 | 0.055 1.51 |
| D570 | Water Absorption, 24 hrs (%) | 0.25 | 0.18 |
| MECHANICAL |
| D638 | Tensile Strength (psi) | 16,500 | 17,000 |
| D638 | Tensile Modulus (psi) | 475,000 | 800,000 |
| D638 | Tensile Elongation at Break (%) | 80 | 3.0 |
| D790 | Flexural Strength (psi) | 20,000 | 30,000 |
| D790 | Flexural Modulus (psi) | 500,000 | 900,000 |
| D695 | Compressive Strength (psi) | 22,000 | 32,000 |
| D695 | Compressive Modulus (psi) | 480,000 | 620,000 |
| D785 | Hardness, Rockwell | M112 / R125 | M114 / R127 |
| D256 | IZOD Notched Impact (ft-lb/in) | 0.5 | 1.0 |
| THERMAL |
| D696 | Coefficient of Linear Thermal Expansion (x 10-5 in./in./°F) | 3.1 | 1.1 |
| D648 | Heat Deflection Temp (°F / °C) at 264 psi | 392 / 200 | 410 / 210 |
| D3418 | Glass Transition Temp (°F / °C) | 419 / 215 | 419 / 215 |
| - | Max Operating Temp (°F / °C) | 340 / 171 | 340 / 171 |
| C177 | Thermal Conductivity (BTU-in/ft²-hr-°F) (x 10-4 cal/cm-sec-°C) | 0.90 3.10 | 0.90 3.10 |
| UL94 | Flammability Rating | V-O | V-O |
| ELECTRICAL |
| D149 | Dielectric Strength (V/mil) short time, 1/8" thick | 830 | 770 |
| D150 | Dielectric Constant at 1 MHz | 3.15 | 3.70 |
| D150 | Dissipation Factor at 1 MHz | 0.0013 | 0.0015 |
| D257 | Volume Resistivity (ohm-cm)at 50% RH | 6.7 x 1017 | 3.0 x 1016 |

The information contained herein are typical values intended for reference and comparison purposes only. They should NOT be used as a basis for design specifications or quality control. 
All values at 73°F (23°C) unless otherwise noted.

ULTEM is a registered trademark of General Electric Company