Vespel® or Meldin® Polyimide Shapes ?

Two great materials, one place to call.

PROFESSIONAL PLASTICS, INC.

Professional Plastics is proud to announce the introduction of Meldin ® 7001 polyimide, a new option for our polyimide customers.  Meldin is initially available in two basic formulations:  Meldin® 7001 (comparable to Vespel SP-1) and Meldin® 7021 (comparable to Vespel SP-21).  The addition of Meldin 7000 series polyimides allows Professional Plastics to provide more options and even better service to our customers.

MELDIN® 7001, Unfilled Grade (brown)
A thermosetting polyimide, Meldin® 7001 is made from the unfilled base resin. This grade offers the maximum mechanical properties and high chemical resistance. The Meldin® 7001 grade is ideal for electrical and thermal insulating applications. More ductile than ceramics, and lighter weight than metals, Meldin® 7001 is a popular choice for structural parts in aerospace & other applications where metal replacement is desirable. 

MELDIN® 7021, 15% by Weight Graphite Filler (black)
Our self-lubricating grade, Meldin® 7021, has 15% by weight graphite fillers, encapsulated by the base polyimide resin. With its low coefficient of friction and high heat resistance, Meldin® 7021 provides our customers the best all-around choice for high temperature bearings, seals, and other low-wear applications.

Comparative Data Sheets for Polyimide Shapes

| Physical Properties | Test Method | Vespel ® SP-1 Unfilled | Meldin ® 7001 Unfilled | Vespel ® SP-21 15% Graphite | Meldin ® 7021 15% Graphite |
| --- | --- | --- | --- | --- | --- |
| Specific Gravity | ASTM D792 | 1.43 | 1.43 | 1.51 | 1.51 |
| Water Absorption | 24 hr. ASTM D570 | 0.24 % | 0.23% | 0.19 % | 0.19% |
| Mechanical Properties@ 73° F |  |
| Hardness, Rockwell E | ASTM D785 | 50 | 40-55 | 35 | 25-40 |
| Tensile Strength, Ultimate | ASTM D638 | 12,500 psi | 12,500 psi | 9,500 psi | 9,500 psi |
| Elongation at Break | ASTM D638 | 7.5 % | 8.0 % | 4.5 % | 3.2% |
| Flexural Modulus | ASTM D790 | 450 ksi | 460 ksi | 550 ksi | 530 ksi |
| Flexural Yield Strength | ASTM D790 | 16,000 psi | 15,800 psi | 16,000 psi | 15,800 psi |
| Compressive Modulus | ASTM D695 | 350 ksi | 380 ksi | 420 ksi |  |
| Electrical Properties |  |
| Surface Resistance | ASTM D257 | 5e+015 ohm | 10 15 – 10 16 ohm | 4.7e+012 ohm | 10 8 – 10 9 ohm |
| Dielectric Constant | at 1 MHz; ASTM D150 | 3.55 | 3.14 | 6.41 |  |
| Dielectric Strength | ASTM D149 | 559 kV/m | 580kV/m | 250 kV/mil | 280kV/m |

For initial test orders, application profiles or qualifying Meldin ® 7000 for your application, call us today !!

Vespel ® is a registered tradename of E.I. DuPont De Nemours   -   Meldin ® is a registered tradename of Saint Gobain Performance Plastics

Contact us at (800) 966-7767   sales@proplas.com     www.professionalplastics.com

# Text boxes

Meldin ® 7000 Series Polyimide Shapes