Vulcanized Fibre (aka Fishpaper)

.

Properties Thickness (inches) Units Commercial Bone Electrical Density .062" grams/cm3 1.20 1.30 1.20 Specific Volume .062" in3/lb 23.0 21.0 23.0 Mechanical Tensile Strength MD .062" psi 16,000 19,000 18,000 CD .062" psi 9,000 9,500 10,000 Modulus of Elasticity in Tension MD .062" psi x 105 12.0 12.0 12.0 CD .062" psi x 105 8.0 8.0 8.0 Flexural Strength MD .062" psi 15,000 15,000 15,000 CD .062" psi 13,000 13,000 13,000 Compressive Strength .062" psi 35,000 35,000 35,000 Impact Strength, Izod Edgewise MD .062" ft-lbs/in. notch 2.0 1.4 2.5 CD .062" ft-lbs/in. notch 1.8 1.0 2.0 Hardness, Rockwell R Scale .062" Divisions 80 100 70 Bond Strength, ASTM D-952 .062" psi 900 1,500 900 Bursting Strength, Mullen .016" psi - - 325 Tear Strength, Elmendorf MD .016" grams - - 550 CD .016" grams - - 700 Electrical Dielectric Strength, Short Time .016" volts/mil 230 - 300 .062" volts/mil 200 200 215 .125" volts/mil 195 200 200 Arc Resistance, ASTM D-495 .062" seconds 80 100 125 Physical Thermal Conductivity, 149° F Btu/hr/ft2/°F/ft. .168 .168 .168 Specific Heat Btu/lb/°F .403 .403 .403 Heat Resistance, Continuous °F 230 - 240 230 - 240 230 - 240 Thermal Expansion x 10-5 MD in/in/°F 1.1 1.1 1.1 CD in/in/°F 1.7 1.7 1.7 Dimensional Change per % change in Moisture Content Thick. % 1.00 1.00 1.00 MD % 0.10 0.10 0.10 CD % 0.25 0.25 0.25 Water Absorption, 24 hours .062" % 66.0 55.0 63.0 Coefficient of Friction, Fibre on Fibre 0.16 0.16 0.16 Coefficient of Friction, Fibre on Smooth Cast Iron 0.21 0.21 0.21 Flammability, ASTM D-635 .062" in/mm 0.5 0.5 0.5

# Text boxes

Need help with your order? Call us at 1-800-966-PROS 
or order online at www.professionalplastics.com today!