PROFESSIONAL PLASTICS, INC.

Phenolic Sheet Thickness Tolerances

At least 90% of the area of the sheet shall be within the tolerances given and at no point shall the thickness vary from the nominal by a value greater than 125% of this specified tolerance. For nominal thickness’ not listed, the tolerance shall be the same for the next greater thickness. For nominal thickness’ greater than 2.0 inches, please contact the Customer Service Department.

| Tolerances in Thickness, Inches |
| --- |
| Nominal Thickness | Paper Based Grades | Cotton Fabric Based Grades | Glass Based Grades | Aramid & Nylon Grades |
|  | NP600 Series | NP310 | NP320 | NP310E | NP320E | NP500 Series | NP100 Series |
| (Inches) | (+ or -) | (+ or -) | (+ or -) | (+ or -) | (+ or -) | (+ or -) | (+ or -) |
| 0.010 | 0.0002 | - | 0.003 | - | - | 0.002 | 0.003 |
| 0.015 | 0.0025 | - | 0.0035 | - | 0.0035 | 0.003 | 0.0035 |
| 0.020 | 0.003 | - | 0.004 | - | 0.004 | 0.004 | 0.004 |
| 0.025 | 0.0035 | - | 0.0045 | 0.005 | 0.0045 | 0.005 | 0.0045 |
| 0.031 | 0.0035 | 0.0065 | 0.005 | 0.0065 | 0.0055 | 0.0065 | 0.0065 |
| 0.047 | 0.0045 | 0.0075 | 0.0055 | 0.0075 | 0.0055 | 0.0075 | 0.0075 |
| 0.062 | 0.005 | 0.0075 | 0.006 | 0.0075 | 0.006 | 0.0075 | 0.0075 |
| 0.094 | 0.007 | 0.009 | 0.007 | 0.009 | 0.007 | 0.009 | 0.009 |
| 0.125 | 0.008 | 0.010 | 0.008 | 0.010 | 0.008 | 0.012 | 0.010 |
| 0.156 | 0.009 | 0.011 | 0.009 | 0.011 | 0.009 | 0.015 | 0.011 |
| 0.188 | 0.010 | 0.0125 | 0.010 | 0.0125 | 0.010 | 0.019 | 0.0125 |
| 0.219 | 0.011 | 0.014 | 0.011 | 0.014 | 0.011 | 0.021 | 0.014 |
|  |  | (+ only) | (+ only) |  |  |  |  |
| 0.250 | 0.012 | 0.030 | 0.024 | 0.015 | 0.012 | 0.022 | 0.015 |
| 0.312 | 0.014 | 0.035 | 0.029 | 0.017 | 0.0145 | 0.026 | 0.024 |
| 0.375 | 0.017 | 0.040 | 0.034 | 0.020 | 0.017 | 0.030 | 0.032 |
| 0.438 | 0.019 | 0.044 | 0.038 | 0.022 | 0.019 | 0.033 | 0.040 |
| 0.500 | 0.021 | 0.048 | 0.042 | 0.024 | 0.021 | 0.036 | 0.048 |
| 0.625 | 0.024 | 0.053 | 0.048 | 0.027 | 0.024 | 0.040 | 0.054 |
| 0.750 | 0.027 | 0.058 | 0.054 | 0.029 | 0.027 | 0.043 | 0.058 |
| 0.875 | 0.030 | 0.062 | 0.060 | 0.031 | 0.030 | 0.046 | 0.062 |
| 1.000 | 0.033 | 0.065 | 0.065 | 0.033 | 0.033 | 0.049 | 0.066 |
| 1.125 | 0.035 | 0.069 | 0.069 | 0.035 | 0.035 | 0.053 | - |
| 1.250 | 0.037 | 0.073 | 0.073 | 0.037 | 0.037 | 0.055 | - |
| 1.375 | 0.039 | 0.077 | 0.077 | 0.039 | 0.039 | 0.058 | - |
| 1.500 | 0.041 | 0.081 | 0.081 | 0.041 | 0.041 | 0.061 | - |
| 1.625 | 0.043 | 0.085 | 0.085 | 0.043 | 0.043 | 0.064 | - |
| 1.750 | 0.045 | 0.089 | 0.089 | 0.045 | 0.045 | 0.067 | - |
| 1.875 | 0.047 | 0.093 | 0.093 | 0.047 | 0.047 | 0.070 | - |
| 2.000 | 0.049 | 0.097 | 0.097 | 0.049 | 0.049 | 0.073 | - |

*Note: For grades NP600, NP602 and NP605, use Glass Tolerances for thickness over 0.125".

Sheet Bow or Twist Tolerance

| All Grades: Thickness, Inches | Max. Bow or Twist *Percent |
| --- | --- |
| 0.031  0.061 | 5.00 |
| 0.062  0.124 | 2.50 |
| 0.125  0.249 | 1.00 |
| 0.250  0.750 | 0.50 |
| 0.751 and over | 0.025 |

*Percentage of  bow is stated in terms of the length or width dimensions; percentage of twist is stated in terms to the dimensions from one corner to the diagonally opposite corner.

Length and Width Tolerances

All sheet sizes: the tolerance in length and width shall be plus or minus 1.0 inch from the nominal trimmed dimensions.

Panels or strips: the tolerance of cut pieces is entirely dependent upon the cutting equipment.

Shearing, sawing, and rotary cutting operations achieve different tolerances. Therefore, the tolerances pertaining to an order will depend upon the cutting operation required. Close tolerances may be possible, but require special attention and equipment.

Cross Reference for ILN Grades - NEMA Grades - Military Specifications

| ANSI/ASTM NEMA LI-1-1998 | Norplex Grade | Military MIL-I-24768/ – Type |
| --- | --- | --- |
| X | NP610 | /12 – PBM |
| XP | NP611, NP660, NP680 | /19 – PBM-P |
| XPC | NP612, NP625, NP664 | /20 – PBM-PC |
| XX | NP629 | /11 – PBG |
| XXP | --- | /21 – PBG-P |
| XXX | NP630 | /10 PBE |
| XXXP | --- | /22 – PBE-P |
| FR-1 | NP691 | /24 – PBM-PF |
| C | NP310 | /16 – FBM |
| CE | NP310E | /14 – FBG |
| CF | NP318 | --- |
| L | NP320 | /15 – FBI |
| LE | NP320E | /13 – FBE |
| G-3 | NP504 | /18 – GPG |
| G-5 | NP509 | /8 – GMG |
| G-9 | NP509 | /1 – GME |
| G-10 | G10 | /2 – GEE |
| FR-4 | NP130, NP130HF, NP510A, NP510AT | /27 – GEE-F |
| G-11 | NP511, MC511A, | /3 – GEB |
| CEM-1 | NP424 | /29 – CEM-1 |
| N-1 | NP101 | /9 – NPG |